## Slide 1: Nanomechanical Damage
Void growth
Void nucleation and hydrogen effects
Fatigue

## Slide 2
Work Completed
Stress, s, is a function
of size.
Work yet to do
Damage f
is a function of stress
and has three components:
1. Nucleation h=h(s,T,e,size)
2. Growth v=v(s,T,e,size)
3. Coalescence c =c(s,T,e,size)
domain of SMM
and LIGA
components
f=hvc
Damage model
Finite element model

## Slide 3
Atomistic Simulations: Consideration of
Boundary Conditions
Case 1: Periodic x,y,z
Dx=Dy=specified
Case 2: Periodic z,
Dx= specified, Dy=linear on x-face
Dy= specified, Dx=linear on y-face
Case 3: Periodic z,
Dx= specified, Dy=free on x-face
Dy= specified, Dx=free on y-face
Case 4: Periodic z,
Dx= specified, Dy=linear on x-face
Dy= specified, Dx=linear on y-face

## Slide 4
Boundary Conditions for one void case do not
matter much for void growth analysis

## Slide 5: Nanoscale Single Crystals Model Setup and Parameters
X
Y
(0 0 1)
(1 0 0)
(0 1 0)
Z

## Slide 6: Nanoscale Single Crystals Model Setup and Parameters for Hydrogen in Ni and Al
X
Y
(0 0 1)
(1 0 0)
(0 1 0)
Z

## Slide 7
Stress-Strain Response of Nickel Lattices
with Hydrogen Atoms
(Same loads are applied in the simulations)

## Slide 8
Stress-Strain Response of Aluminum Lattices with Hydrogen Atoms
(Same loads are applied in the simulations)

## Slide 9: Size Scale Effects of Stress-Strain Response

## Slide 10
Fracture Strain and Stress vs Hydrogen
Atomic Concentration
The effect of hydrogen on crack growth susceptibility in a number of alloy systems
exhibit limiting values at high concentrations. (Moody, 1990)

## Slide 11
6 nm/0.5%H
Strain 0.05
12 nm/0.5%H
Strain 0.05
24 nm/0.5%H
Strain 0.05
48nm/0.5%H
Strain 0.05
Size Scale effects of dislocation cell
structures with hydrogen effects

## Slide 12: The Number of Dislocation Cells vs True Strain

## Slide 13: Orientation A [111] with initial crack-note closure
Cycle 2
Cycle 4
Cycle 5
Cycle 6
Cycle 7
Cycle 8

## Slide 14: Orientation B – [100] with initial crack: note isotropic like plasticity
Cycle 3
Cycle 4
Cycle 5
Cycle 7
Cycle 8
Cycle 9

## Slide 15: Orientation C – [110] with initial crack: distributed plasticity
Cycle 3
Cycle 4
Cycle 6
Cycle 9
Cycle 11
Cycle 12

## Slide 16: Orientation D – [101] with initial crack: note shear bands
Cycle 2
Cycle 3
Cycle 5
Cycle 6
Cycle 9
Cycle 10