Chapter 6

Measuring Surface Reduction from Leached Sulfate.

In Eq. 6-19, the calcium ion is expressed as mol/liter, where as Eq. 6-20 is expressed as surface reduction in  m/m of rain fall. Here, the details of the conversion calculation is shown.

Let, C  = concentration of Ca+2,  mol/liter

M= molecular weight of CaCO3

 = density of calcite (gm/cm3)

RF = rain fall, cm

A = exposed sample surface area, cm2

SA= total sample surface area, cm2

From the concentration the following relation converts it to volume of material:

CMρ×RF×A...........................(1)

Using the actual surface area, Eq(1) can be rewritten as

=C×Mρ×RF×ASA.........................(2)

If all the surface of the sample is exposed to rain, then SA=A in Eq. (2). As RF is the rain fall in cm, Eq. (2) can be used to get surface recession per cm of rain fall. This is given by Eq.(3):

=C×Mρ×RF×SASA×RF........................(3)

Equation (3) gives the surface recession per cm of rain fall.

For example, if the leaching was 0.15 mol/liter of  Ca2+ , the surface reduction can be obtained as follows:

C= (0.15/1000)*100.09 gm/liter =0.015 gm/liter

M= 100.09,  = 2.74

Total dissolution = 0.015/(1000)*(1/2.74) SA*R

=5.47*10-6 SA*R cm3

Surface recession for R (cm) rainfall	= 5.47*10-6 SA*R/SA  cm

Surface recession per meter of rain  =5.47*10-4 cm

So, the surface reduction  will be 5.47 m per meter of rain fall.