The incomplete Problem 15.1 now shown on the ftp site is given below:

15.1. The solidification and cooling of pure Mn is a complex sequence of phase changes and volume changes. (a) Assume that a specimen of liquid Mn has a volume of 1000.0 cm3 at the melting temperature of 1244˚C. Use the following information about Mn allotropes to construct a plot of volume (y-axis) versus temperature (x-axis) for this specimen as it cools to 20˚C. Label on your plot the final value of specimen volume at 20˚C.

Correct Problem 15.1 is given below.  Please use this on the ftp site.:

The solidification and cooling of pure Mn is a complex sequence of phase changes and volume changes. (a) Assume that a specimen of liquid Mn has a volume of 1000.0 cm3 at the melting temperature of 1244˚ C. Use the following information about Mn allotropes to construct a plot of volume (y-axis) vs. temperature (x-axis) for this specimen as it cools to 20˚ C. Label on your plot the final value of specimen volume at 20˚ C.

Phase	Coefficient of thermal expansion (mm/mm·C˚)

	41.6(10-6)

	14.8(10-6)

	24.9(10-6)

	22.3(10-6)

Phase transformation	volume change (%)

liq	-2.9

 	-0.8

 	-0.8

 	-3.4

(b) Predict whether or not each of the four transformations during cooling (liq) would be likely to crack the specimen. Justify your answers.

(c) The FCC structure of -Mn is a "densest-packed" crystal structure. Yet Mn'stransformation results in a contraction (negative volume change). Explain how it is possible for the Mn atoms to become more densely packed than their FCC packing efficiency.