Problems

1.1. The crystal structure for Fr is unknown because all its isotopes are radioactive, and its longest-lived isotope has a half-life of only 21 minutes. It would be extremely difficult to produce, concentrate, and purify a sufficient quantity of the element rapidly enough to allow diffraction analysis, and even if that were accomplished somehow, the sample would have a strong tendency to melt itself from its own decay heat. (a) Write a short paragraph describing your prediction of what crystal structure(s) Fr might be expected to have if it could be produced in sufficient quantities for diffraction analysis. Defend your conclusions based on Fr’s position in the periodic table. (b)  Like Fr, element 112 is also radioactive, and its isotopes have even shorter half-lives (< 1 ms). Write a short paragraph describing your best prediction of the crystal structure(s) this element might be expected to have if it could be produced in significant quantities and kept from vaporizing itself from its own decay heat. Defend your conclusions based on this element’s position in the periodic table.

1.2. The enormous pressures used to study the high-pressure crystal structures of the elements substantially increase the material's density. Figure 1.11c indicates that Al will transform to the BCC structure at an atomic volume of 35% of the original atomic volume. (a) Assuming that spherical atoms exist in that BCC Al structure, calculate the density of BCC Al with atoms whose volume is 35% that of FCC Al atoms. (b) How does this density compare to that of FCC Al at ambient pressures?

1.3. Po is the only element with a simple cubic structure under ambient conditions. Its density is 9.14 g/cm3. (a)  Make a pictorial drawing of the unit cell of -Po (cP1). (b)  How many nearest-neighbor atoms are present in this structure? (c)  How many second-nearest-neighbor atoms are present in this structure? (d)  Determine the Miller indices of the most densely packed crystal plane in -Po, and calculate the area density of that plane. (Area density is the number of atoms whose nuclei lie exactly on the plane divided by the plane's area.)

1.4. Several tC2 crystal structures exist; make a pictorial sketch of one such structure.

1.5. Of the crystal structures cI2, hP2, cF8, cP1, hP4, and tI2 (a) which are cubic structures and (b) which are densest-packed structures? (c) For each structure listed, give an example of a pure metallic element that has that structure at ambient pressure and temperature.

1.6. The atomic volume of Ni is 0.01094 nm3, and the atomic volume of Pd is 0.01472 nm3. Thus, the atomic volume increases 34.6% by moving down one position in group 10. The atomic volume of Pt is 0.01510 nm3; this is only slightly larger than that of Pd (because of the lanthanide contraction). Estimate the density that Pt metal would have if there were no lanthanide contraction. This can be done by assuming an atomic volume of Pt that is 34.6% larger than the atomic volume of Pd and then computing a new density for Pt based on that larger Pt atom.

1.7. The use of depleted U for armor-penetrating projectiles has been controversial because U is both a radiological and a chemical toxin. When these shells are used, much of their U is converted to fine dust by explosions and fires. U dust contaminates battlefields long after combat ends, causing unintended harm to combatants and civilians. Use Fig. 1.13 to suggest other high-density metals that might be practical substitutes for depleted U in projectiles. Justify your recommendations in terms of density, cost, toxicity, and mechanical properties.

1.8. Th metal transforms from FCC to BCC crystal structure at 1633 K. Calculate the percent density change that accompanies this transformation.

1.9. Lanthanides with higher atomic numbers (e.g., Er, Tm, Lu) have substantially greater densities than lanthanides with lower atomic numbers (e.g., Ce, Pr, Nd). This results from the fact that the higher-atomic-number lanthanide atoms are both smaller and have greater mass. Calculate which of these two effects (atomic size, mass) has the greater influence on the increase in density seen in the higher-atomic-number lanthanides.

1.10. Al has hybridized bonding. (a) Describe the ground state of the electrons in a single Al atom that is not bonded to any other atoms. (b) Describe the hybridized state of the electrons in an Al atom that is part of a pure Al crystal. (c) How many electrons are available for bonding in each of these two configurations?  (d) Would the strength of Al metal be higher or lower if Al’s bonding were not hybridized?

2.1. In a typical metal, the energy of formation of a vacancy is 1 eV, and the energy of formation of a self-interstitial atom is 5 eV. Use equation (2.1) to predict the vacancy defects/self-interstitial defects equilibrium ratio in such a metal at 1000 K.

2.2. Some intermetallic compounds compensate for off-stoichiometric compositions by creating large numbers of vacancies in the lattice. NiAl, for example, has been observed to have up to 6% of its Ni lattice sites vacant when the composition is Al-rich (e.g., 53% Al–47% Ni). The material accommodates the “shortage” of Ni atoms by leaving some of the Ni sites vacant. Use your knowledge of defect interactions to predict what effect this high vacancy concentration would have on the strength of Al-rich NiAl. Specifically, would the high vacancy concentration make the metal stronger, weaker, or cause no significant change in strength? Justify your answer.

2.3. The energy of formation of a vacancy in pure Al is 0.67 eV. (a) Use equation (2.1) to predict the equilibrium vacancy concentration (Nd/N) for Al at 77 K. (b) If a 1-kg ingot of pure Al is cooled to 77 K, determine how many lattice sites will be vacant if it contains the equilibrium concentration of vacancies calculated in part (a). Comment on the reasonableness of this answer. What prevents the metal from achieving the equilibrium number of vacancies at 77 K?

2.4. The energy necessary to produce a dislocation is proportional to the square of the Burgers vector length (b2). Therefore, the lowest-energy dislocations are those having the shortest Burgers vector. For an HCP metal with an “ideal” c/a ratio of 1.633, calculate which slip direction would have lower energy, the 13<1120> or the 13<1123> (see Fig. 11.2).

2.5. A dislocation lying parallel to the [010] direction in a cubic crystal has a Burgers vector parallel to the [111] direction. Is this an edge, screw, or mixed dislocation?

2.6. (a) In a low-angle tilt boundary, are the dislocations that comprise the boundary edge type or screw type? Do they have their Burgers vectors generally parallel or perpendicular to the boundary plane? (b) In a low-angle twist boundary, are the dislocations edge type or screw type? Do they have their Burgers vectors generally parallel or perpendicular to the boundary plane?

2.7. Figure 18.32 shows preferred orientation in a cold-drawn Au wire. A disproportionately large number of the grains in this Au wire have their {111} planes nearly perpendicular to the wire’s length (i.e., most grains have a <111> direction parallel to the wire’s length). The {111} plane is the slip plane in Au. The {111} planes lying perpendicular to the wire axis will experience low resolved shear stresses for slip if this Au wire is pulled in tension along its length. Will this texture make it difficult for the wire to slip, causing low ductility compared to a wire with randomly oriented grains? Explain your answer.

2.8. Formation of a twin boundary during deformation moves the atoms in the twinned region with respect to the untwinned metal. (a) Is diffusion necessary in order to accomplish this atom motion? Explain your answer. (b) Is a twin boundary a barrier to motion of an edge dislocation? Explain your answer.

2.9. Identify the type of planar defect present in each of the following stacking sequences for a FCC metal: (a) . . . ABCABCBACBA . . . , and (b) . . . ABCABCBCABC . . . .

2.10. The vacancy formation energies of some pure BCC metals are tabulated below. Calculate the vacancy concentration (Nv/N) for each metal at 50%, 60%, 70%, 80%, and 90% of its absolute melting temperature, and plot the results of your calculations on a semilog graph of homologous temperature (x-axis) versus vacancy concentration (y-axis, log). Comment on the similarities and differences observed between the four metals.

| Element | Vacancy Formation Energy (eV) |
| --- | --- |
| W | 3.6 |
| Ta | 3.1 |
| V | 2.2 |
| Li | 0.48 |

3.1. A plate of 99.95% pure Ni (Tm.pt. = 1728 K) was annealed at 1273 K for 18 hours, then cold-rolled to a 2% reduction in thickness. Following the cold rolling, the metal was annealed for 2 hours at 864 K to recrystallize it. However, metallographic examination of the grain structure performed both before and after the 864 K anneal showed that no recrystallization occurred during this anneal. Briefly explain (50 words or fewer) why the metal failed to recrystallize.

3.2. Al alloy I-beams are purchased from an extrusion and heat treatment subcontractor (company X) for use by company Y in fabricating the load bed of a large truck. The beams were to be made of a precipitation-hardening Al alloy, and company X was instructed to deliver the beams to company Y in a precipitation-hardened condition. A few weeks after the first trucks made by company Y were sold and put into service, customers begin to file complaints that these beams were bending when loaded in service. The beams did not straighten when the load was removed; they were deformed permanently. Assume that you are called upon to diagnose what went wrong. Make a list of five things that could have caused the beams to deform.

3.3. The table below presents grain size and yield strength measurements for three Cu–Zn solid solution alloy specimens. All three specimens had the same composition. Calculate a predicted value for the missing yield strength datum indicated by the “?”.

| Grain Size (m) | Tensile Yield Strength (MPa) |
| --- | --- |
| 100 | 68 |
| 10 | 150 |
| 5 | ? |

3.4 (a) To calculate the dislocation density that would be needed in Cu to raise the tensile yield strength to 275 MPa, the value considered to be "half-hard" for cold-worked Cu, use Gb1/2, where  is the yield stress (MPa);  a dimensionless constant, ≈ 0.5; G is the shear modulus (MPa); b is the length of the Burgers vector (cm); and  is the dislocation density (cm-2). (b) If dislocations lie parallel to one another and are spaced uniformly in the metal, calculate the spacing between the dislocations needed to produce the dislocation density determined in part (a).

3.5. The table below shows the solid-solution strengthening effect of various solutes in Cu. (a) Calculate the size mismatch in percent to complete the third column in the table. (b) Calculate the correlation coefficient between the values in column 3 and the values in column 4. Assume percent size mismatch to be the independent variable and slope to be the dependent variable. (c) Briefly describe factors other than atomic radius that could affect the ability of a given solute atom to harden Cu — that is, explain why the correlation coefficient is not 1.

| Element | Atomic Radius (nm) | Percent Size Mismatch | Increase in y of Cu per Atomic % Solute Added (y of Pure Cu = 70 MPa) |
| --- | --- | --- | --- |
| Cu | 0.128 | – | – |
| Sn | 0.151 |  | 17.5 |
| Be | 0.114 |  | 8.75 |
| Si | 0.118 |  | 4.18 |
| Al | 0.143 |  | 3.57 |
| Ni | 0.125 |  | 2.66 |
| Zn | 0.133 |  | 1.36 |

3.6. Assume that you are asked to describe the four strengthening mechanisms in metals to a corporate vice president who is not trained in engineering or science. Write one paragraph and make one sketch to illustrate these concepts briefly and simply for the vice president. If you use terminology not usually familiar to a layperson, you will need to define those terms in your paragraphs.

3.7. If the grain growth phase following recrystallization is allowed to proceed for an extremely long time (i.e., one year at 0.9Tm.pt.), the grains grow to a larger average grain size, but the specimen does not become a single crystal. Why doesn’t a single crystal eventually result?

3.8. The phase diagram shown in Fig. 11.9 for Mg–Al appears to be well suited to precipitation-hardening reactions; note how closely it resembles Fig. 20.13. However, when one attempts to precipitation harden an alloy such as Al–5% Mg, the strength of the optimally aged alloy is only slightly higher than the strength of as-quenched metal. Present two possible explanations for this disappointing lack of strengthening response in this alloy.

3.9. The Friedel relation suggests that the shear stress needed for flow (c) should vary with the square root of the foreign atom concentration (i.e., c1/2). Ni can hold up to 60 at% Co in solid solution. Design and describe an experiment to determine whether the Friedel relationship is valid for a Ni–Co solid solution alloy. Your description of the experiment should be sufficiently detailed that you could give it to a competent technician and have him or her perform the entire experiment without having to ask you further questions.

3.10. During field assembly of some precipitation-hardened Al alloy struts on an unmanned aircraft, the holes for a threaded fastener fail to align well enough to allow a bolt to be passed through both holes. A mechanic says he has a helium-shielded arc welding rig available, and he suggests arc-welding the two struts together to fasten them without using the bolt. Write a brief assessment of whether this is a good solution to the misfit problem from a metallurgical perspective.

4.1. Estimate the shear stress acting on bowed dislocation segment XY shown in Fig. 7.13e. Assume that  = 0.7, the shear modulus of Cu is 44 GPa, the dislocation is parallel to the image plane of Fig. 7.13e, and that the dislocation is a perfect 1/2111<101> dislocation.

4.2. Estimate the stacking fault width between two a6<211>- type partial dislocations in Al, which has a stacking fault energy of 150 mJ/m2.

4.3. Es has the -La crystal structure (Fig. 1.2d). Due to the short radioactive decay half-life of Es, no single crystals of the metal have ever been grown for tensile testing. Predict the most likely slip system (plane and direction) for deformation of Es and justify your prediction. You may find the information in Appendix A and Appendix B1 helpful in answering this question.

4.4. A screw dislocation containing an edge-character jog has difficulty moving through a metal's lattice; however, such dislocations move more readily in metal that has been irradiated extensively with high-energy particles (Sec. 7.5). Explain why irradiation facilitates motion of such dislocations.

4.5. Equation (4.13) and Fig. 4.9 describe the separation of a perfect dislocation into two partial dislocations on the {111} planes of a FCC metal. The same atom arrangement occurs on the (0001) plane of an HCP metal. Determine the vector expression for the perfect dislocation that would dissociate into two partial dislocations in the reaction:

13[????]→13[0110]+13[1100].

4.6. Write a short paragraph (200 words or fewer) to explain (a) why the slope of the curve for region I is much lower than the slope of the curve for region II in Fig. 4.16, and (b) what causes the crystal to change from region I–type deformation to region II–type deformation. That is, why doesn't region I behavior continue until the metal fractures?

4.7. If a single crystal of Zn is tensile tested with its (0001) plane perpendicular to the direction of the tensile force, the Schmid factor for slip on the (0001) plane is zero. Describe three possible responses such a Zn single crystal could make in response to such a load.

4.8. If CRSS = 5.0 MPa for {111}<110> slip in Ni, calculate the tensile stress needed to initiate slip on the {111}<110> slip system if a Ni single crystal is tested with the tensile axis parallel to the <001> direction.

4.9. Assume that 1.0 kg of cartridge brass (an FCC solid solution alloy comprised of 70 wt% Cu–30 wt% Zn) has been cold-worked to achieve a dislocation density (perfect basis) of 1.0(1012) cm-2. Further assume that all these dislocations are separated into pairs of partial dislocations with stacking faults lying between the partials [i.e., the partial dislocation density is 2.0(1012) cm-2]. Use Fig. 18.17 to assist you in estimating the total area (in square centimeters) of such stacking faults in the alloy.

4.10. A single crystal of Mo is tensile tested with the tensile axis parallel to the [111] direction. (a) Calculate the Schmid factor (cos  cos ) for slip on the (121) plane in the [111] direction for this tensile orientation. (b) There are other combinations of {211} planes and <111> directions with higher Schmid factors for this tensile orientation. Identify one such plane-direction combination and calculate its Schmid factor.

5.1. A large plate of a completely brittle material is put under 85 MPa of tensile stress. The Young’s modulus of this material is 140 GPa, and its surface energy is 450 mJ/m2. A crack exists at the edge of the plate with the plane of the crack perpendicular to the tensile stress. Use the Griffith equation to calculate the maximum crack depth that can be tolerated without fracturing the plate under the 85-MPa tensile stress.

5.2. ASTM KIC fracture toughness values allow estimation of the critical crack size in parts whose thickness is sufficient to result in plane strain behavior according to KIC=Yspa, where Y is a stress intensity factor that is near 1 for shallow cracks in wide plates,  the applied tensile stress, and a the crack depth. Use this formula to plot the relation between KIC and critical crack depth (a) for a plate under a 200-MPa tensile load. Assume that Y = 1, and assume that the crack is on the plate edge rather than internal. Plot values of KIC over a range of 80 MPa√m (typical for many steels) to 4 MPa√m (common for several intermetallic compounds).

5.3. An Al alloy structural member contains a 1.0-mm-deep crack at its edge. The member  has a stress intensity factor (Y) of 1.22, and it will be loaded to 250 MPa in service. (a) This alloy has a plane strain fracture toughness of 35 MPa√m. Use the equation provided in problem 5.2 to calculate whether the crack will cause the member to fail when it is loaded.  (b) The designers of this part want to maintain a safety factor of 2 for this member (i.e., the part should be able to carry a load that is double the actual load expected in service). Does this part provide a safety factor of 2 when the expected load is 250 MPa?

5.4. Os is a brittle metal at room temperature, and even when heated to 1200˚C it still will not plastically deform. Assume that you are asked by your supervisor to find some set of conditions under which Os will display at least a few percent elongation in a tensile test. Briefly describe four or five experimental conditions that would improve the probability of achieving a few percent elongation in a tensile test.

5.5. Fatigue test data for a Cu–Zn alloy are shown in the table below. (a) Make an S/N plot of these data and use your plot to predict the fatigue strength at 6 x 105 cycles. (b) Does this metal display a classic fatigue limit?

| Stress Amplitude (MPa) | Cycles to Failure |
| --- | --- |
| 313 | 3(105) |
| 220 | 1(106) |
| 194 | 3(106) |
| 171 | 1(107) |
| 152 | 3(107) |
| 143 | 1(108) |
| 135 | 3(108) |
| 126 | 1(109) |

5.6. Intermetallic compounds containing Al (e.g., AlFe and NiAl) often show little or no ductility in tensile tests on polycrystalline material, failing by intergranular fracture before appreciable plastic flow occurs. One theory proposed to explain this behavior is that Al causes H2O vapor to decompose at its surface by the reaction 2Al + 3H2O  6H + Al2O3. The H atoms from this reaction then diffuse along cracks and grain boundaries, embrittling the metal adjacent to both of these defects. (a) Write a paragraph describing an experiment that could be performed to test the validity of this theory. (b) Pure Al is highly ductile. If this theory is proven to be valid by your experiment, suggest one or two reasons why the reaction above does not embrittle pure Al metal. You may find Secs. 20.2.2.1, 20.2.2.6, and 25.6.1 helpful in answering this question.

5.7. Two fatigue tests are performed on a Ti alloy with a yield strength of 900 MPa. In the first test, the applied load cycles between 300 MPa in compression and 600 MPa in compression. In the second test, the applied load cycles between 300 MPa in tension and 600 MPa in tension. Predict which test will fracture the Ti with fewer load cycles. Justify your prediction.

5.8. In the early twentieth century, it was widely believed that fatigue failure occurred when metal “crystallized” from repeated elastic straining. Once crystallized, the metal was thought to cleave along its newly formed crystal planes. That theory has long since been abandoned by materials engineers, but it is still sometimes invoked by those whose knowledge of materials science is not “up to date”. Assume that you receive an e-mail from a nonmaterials science colleague who is working on a system that is experiencing fatigue failure problems. His message to you says that he has heard that metal crystallizes under stress, and he asks your advice on how to keep the metal in his system from crystallizing. Compose an e-mail reply (150-word maximum length) to this inquiry that will help your colleague understand modern theories of fatigue.

5.9. The landing gear of a commercial aircraft may experience five landings per day in normal service. An intake valve in an automobile's internal combustion engine may experience 1500 loading and unloading cycles per minute during the one hour per day that it operates. How long will it take each part to reach an N value of 1(106) cycles?

5.10. A satellite in low Earth orbit has an orbital period of 90 minutes, and it enters and exits Earth's shadow once during each orbit. A rigidly constrained Be strut cools to –115˚C when it is in Earth's shadow, and it warms to 85˚C when it is in sunlight. If the strut has no stress when it is at a temperature of 22˚C, determine (a) whether the strut will reach its yield strength of 480 MPa, and (b) whether there is a realistic concern about a possible fatigue failure during this component's expected 10-year service life in orbit.

6.1. Assume that a pure Ta grain like the one depicted in Fig. 6.5 is undergoing Coble creep. If the grain is a cube with a 10.0-m edge length, how many vacancies must move from the upper and lower grain boundaries to the four vertical grain boundaries to make the grain 11.0 m tall?

6.2. If an atom requires 1.0 eV to jump out of its lattice site to form a vacant neighboring lattice site, calculate whether that energy is larger than, about equal to, or smaller than the mean thermal vibration energy of atoms at 300 K. If your answer was “larger than” or “about equal to,” explain why diffusion requires long times to change concentrations in metals at room temperature. If your answer was “smaller than,” explain why the diffusion rate in metals at room temperature is not zero.

6.3. The Nb–O alloy tensile tested to produce Fig. 13.7 undergoes dynamic strain aging at 250˚C but not at room temperature. Predict whether this alloy would have higher or lower ductility at 250˚C than it would have at room temperature. Justify your answer.

6.4. If a study performed on creep specimens determines that the relationship between strain rate (e.) and average grain size (d) ise.µd−2.5, would you conclude from this result that the creep was occurring by Coble creep, Nabarro–Herring creep, or a combination of both types of creep? Explain your answer.

6.5. Referring to the deformation map shown in Fig. 6.6, there is no region labeled “diffusion creep.” If you were to place such a label on this map, where would it properly reside?

6.6. Make a sketch of the grain structure you would expect to see if you examined a polished, etched metallographic specimen from the gauge-length metal in each of the two tensile test specimens shown in Fig. 6.7. Place an approximate scale bar on each of your two sketches.

6.7. (a) Use equation (6.4) to plot a graph of the strain rate (y-axis) versus grain size (x-axis) of a pure Cu creep specimen tested at 850˚C under a load of 1.2 MPa. Plot values for grain sizes ranging from 1 to 100 m. For self-diffusion in Cu, D0 is 7.8 x 10-5 m2/s and Q is 211 kJ/mol. (b) Use the plot you developed in part (a) to predict how long it would take a pure Cu specimen with a 3.0-m grain diameter to elongate 10% when loaded at 1.2 MPa at 850˚C.

6.8. Although few parts subject to creep strain are ever used deliberately in their tertiary phase of deformation, engineers are still interested in this creep phase. Briefly describe (in about 50 words) the safety considerations that make the tertiary-phase behavior a matter of design interest.

6.9. Wire drawing is used routinely to produce fine wires with diameters of about 10 m and sometimes as fine as 2 m. However, drawing wire to diameters ≤ 1 m poses several processing challenges involving workpiece handling and fabrication of dies with such exceptionally small hole diameters. Assume your supervisor asks you to use superplastic forming (Secs. 8.4.5 and 19.2.6) to elongate 2 m diameter wire to achieve a diameter of 500 nm. Write a paragraph discussing whether this idea has a reasonable prospect of producing 500-nm-diameter wire successfully.

6.10. A strain rate jump test can be used to measure the strain rate sensitivity of a metal. In this test the tensile specimen is pulled to 2% elongation, and at that point the strain rate of the test is abruptly increased, typically by a factor of about 100. The stress needed to continue the deformation at the higher strain rate usually increases, as shown by the “steps” in Fig. PS6.3. The strain rate sensitivity, m, can be determined in such a test with the equation

m=lns2s1lne2e1

where  is the tensile stress and e is the strain rate. The two stress–strain curves shown in Fig. PS6.3 were made by subjecting two specimens of identical composition and grain size to a strain rate jump test at the temperatures indicated. In each test the jump was from an initial strain rate of 8.2(10-5) to a strain rate of 4.1(10-3) s-1. Based on these test results, predict which of these temperatures is likely to work better for superplastic forming of this alloy. Explain the reasoning behind your answer.

7.1.  Assuming that the high-angle grain boundary energy of Cu is 6.0(102) mJ/m2, calculate the total grain boundary energy of 1.0 g of (a) nanocrystalline Cu with a grain size of 5.0(101) nm, and (b) nanocrystalline Cu with a grain size of 5.0 nm. Use the simplifying assumption that the grains are cube shaped. (c) If all the grain boundary energy of the metal in parts (a) and (b) were suddenly converted to thermal energy, calculate the temperature rise that this would cause in each of the two Cu samples.

7.2. Estimate the toughness in J/m3 of the two Ni specimens whose tensile data are plotted in Fig. 7.3.

7.3. Use the data in Table 7.1 to estimate the modulus of resilience of Vitreloy-1 in J/m3. Compare your result to the estimated modulus of resilience of half-hard, cold-worked 304 austenitic stainless steel, which has y, 0.2% = 760 MPa at an elastic strain limit of 0.5% elongation.

7.4. Quasicrystalline materials usually have high hardness and a low coefficient of friction. Their use to date has been limited to boutique applications such as cookware and electric razors. Describe three other applications where these two properties of quasicrystalline materials could be used to good advantage.

7.5. It is possible to cover a flat surface with regular (i.e., equiangular and equilateral) hexagons such that all the area is covered and there is no overlap of the hexagons. Calculate the internal angles of a regular pentagon and show arithmetically why it is impossible to tile a flat surface with pentagons such that all the area is covered and there is no overlap of the pentagons.

7.6. Amorphous metals can be made into foams by bubbling gas through the viscous, liquid alloy; as the metal cools, its viscosity increases greatly, producing a rigid mass. Alternatively, the amorphous metal can be “foamed” by melt infiltration into hollow C spheres.  These processes produce highly porous metals (in some cases up to 99% porosity). Describe three practical uses for such a foamed metal.

7.7. Fusion reactions produce neutrons with kinetic energies of 14 MeV. (a) If this energy is used with 100% conversion efficiency to produce equal numbers of vacancies and interstitial defects in a metal target, estimate the total number of defects that would be generated by one 14-MeV neutron. (b) Explain briefly why this estimation is unrealistic.

7.8. The stacking fault shown in Fig. 4.13 is an edge dislocation loop. Would this stacking fault loop be able to enlarge its radius under an applied shear stress and cause slip in the crystal in the same way that dislocation loops from a Frank–Read source (Sec. 4.4) can expand and cause slip? Justify your answer.

7.9.  Examine a collection of binary equilibrium phase diagrams and suggest a possible binary alloy other than Au–Si that would have favorable characteristics for forming an amorphous metal upon rapid quenching from the liquid phase, as by splat cooling. Explain why you chose the composition you are recommending.

8.1. Casting operations would benefit from the hard vacuum and microgravity of space, but new problems would also arise. Write a 100- to 300-word description of some advantages and disadvantages of performing casting operations in an orbiting space station compared with the same operation done terrestrially.

8.2. The process of converting massive metal into powder involves forming a new metal–air interface area. These surfaces have energy associated with them. (a) If Al metal has a surface energy of 1.2 J/m2, calculate the surface energy requirement associated with converting a 1.0-kg sphere of pure Al into spherical powder particles of pure Al having a diameter of 25 m.  (b) How does this energy compare with the energy needed to melt the initial 1.0-kg sphere of Al? (c) Calculate the surface energy requirement associated with converting a 1.0-kg sphere of pure Al into spherical powder particles of pure Al having a diameter of 25 nm.

8.3. In the mid-twentieth century, Hg metal was sometimes used for investment casting patterns; however, this practice has been discontinued. Why?

8.4. Flame cutting of steel is widely used to make fast, rough cuts on thick steel plate, but the process works poorly for Ti plates.  Suggest two reasons why flame cutting is ill suited to cutting Ti.

8.5. Resistance welding is more difficult on Cu than on other metals due, to Cu’s low electrical resistivity. (a) For the heat generated in a resistance welding operation, compare the ratio of current needed to generate the same amount of heat in pure Cu and pure Ni workpieces, assuming that part geometry and all other variables are equal, using H = RI2t, where H is the heat generated by the current pulse, R the resistance of the workpiece in ohms, I the current amperage, and t the time duration of the pulse. (b) There is another factor that makes Cu difficult to join with resistance welding. Provide a one-sentence description of this second factor.

8.6. A solid Nb cylindrical workpiece containing 3200 ppm O is 75 mm high and 5.0(101) mm in diameter. This workpiece is to be open-die forged (Fig. 8.12) at 250˚C with flat dies to reduce its height to 7.0(101) mm. Assuming that the coefficient of friction between the dies and the workpiece is 0.25, calculate the forging force needed for this process. Refer to Fig. 13.7 to estimate the maximum flow stress of the material during this reduction.

8.7. A 3.0-mm-thick sheet of Be metal displayed an 8.0% reduction in area in a tensile test. If it desired to bend this Be sheet into a cylindrical wall for a fuel tank, what is the smallest diameter that fuel tank could have without cracking the Be during the bending operation?

8.8.  Cutting tools generate heat in use. Refer to Chapter 16 to determine the temperature at which WC–Co cermet composite cutting tool strength would be reduced to zero. Briefly explain why the tool would fail at this temperature.

The Co-W-C ternary system forms an eutectic at 1275˚ C (Sec. 16.2.3.3). Once a liquid phase forms in a cutting tool, its strength becomes essentially zero because the remaining solid phases present in the cutting tool are no longer bound to one another.

8.9. A technician is attempting to join Ti plates to Co plates. Despite repeated attempts with various power settings and feed rates, all efforts to join the plates by inert-gas shielded arc welding have failed due to cracking in the metal as it cools after welding. The technician comes to you in frustration and says this process is not working and asks you if he should try electron beam welding to join these two plates. (a) Use Fig. 25.7 to explain why the welded metal is cracking, and (b) give your opinion of the probability of success in electron beam welding these two metals. (c) Suggest two other alternative joining methods that would have a good probability of accomplishing this task.

8.10. CaO-stabililized ZrO2 can be thermal sprayed onto metal parts to provide them with an oxidation-resistant, thermal barrier coating. The coefficient of thermal expansion (COTE) of CaO-stabililized ZrO2 is 10.1 m/m·K. For which of the metals Al, Cu, gray cast iron, Ta, Ti, W, and Zn does the COTE of CaO-stabilized ZrO2 come within 20% of the COTE of the metal?

9.1. (a) Use the Miller–Humphreys expression in equation (9.2) to calculate the increase in dislocation density that occurs in the matrix of an 80.0 vol% Cu–20.0 vol% W particle composite when it is cooled from 20˚C to -196˚C by immersing it in liquid N2. Assume that the W particles are cube-shaped and are 20.0 m on each edge. (b) Estimate the increase in Cu’s yield strength resulting from the dislocation density increase caused by this LN2 immersion.

9.2. It is possible to produce a composite tensile test specimen that has reinforcing filaments running the entire specimen length and oriented parallel to the tensile axis. In such a composite, there are no “end effects” on the filaments, and the elastic strains in the filaments, the matrix, and the composite will all be equal for the elastic regime. Derive a variation of equation (9.1) for this situation that expresses the Young’s modulus of the composite as a function of the volume fraction of the filaments, the Young’s modulus of the filament material, and the Young’s modulus of the matrix material.

9.3. A continuous, aligned fiber MMC contains 25 vol% reinforcing fibers. This composite is loaded parallel to the fibers’ axes, and the load is less than the load needed to reach the yield stress of the composite. The reinforcing fibers are carrying 75% of the total load applied to the composite. Calculate the Ef/Em ratio, where Ef = the elastic modulus of the reinforcement fiber, and Em is the elastic modulus of the matrix.

9.4. Figure 9.5 seems to suggest that the best way to produce a composite with a high strength-to-weight ratio would be to pair an exceptionally strong reinforcing material with a very light matrix metal. For example, a Li metal matrix (density 0.54 g/cm3, strength near zero) containing 50 vol% continuous, aligned B filaments (density = 2.6 g/cm3, strength 7000 MPa), would appear to have an average strength parallel to the filament axes of 3500 MPa and a density of only 1.57 g/cm3. Describe briefly the flaw in this line of reasoning to explain why such a composite will not have a strength of 3500 MPa.

9.5. Use the shear lag model to estimate the maximum length of 60-m-diameter graphite filaments that can be used without filament fracture in a pure Ni matrix (Sec. 16.3.2.2).

9.6. As Fig. 9.12 illustrates, Ti MMCs have large performance advantages over ordinary Ti alloys, particularly at elevated temperatures. The largest drawback to use of Ti MMCs is their high cost. Suggest three applications where the high cost of Ti MMCs might be expected to be recovered by lower operating costs and/or longer part lifetimes.

9.7. Figure 20.16 indicates that the Orowan dislocation looping shown in Fig. 9.6 becomes progressively more difficult to accomplish as the particle size becomes smaller. This suggests that a logical method to increase composite strength would be to make composites with much smaller reinforcement particles. Write a paragraph explaining why composites with exceptionally small reinforcement particles are difficult to produce.

9.8. Residual stress from a difference in the coefficients of thermal expansion (COTEs) of the matrix and reinforcement phases can degrade the mechanical properties of a composite (Fig. 9.7). Use Table 9.1 and other materials properties information to suggest three metal matrix composite compositions that would have matrix and reinforcement materials with nearly equal COTEs.

9.9. One idea put forth for achieving exceedingly small oxide dispersions that are distributed uniformly in a MMC is to heat-treat a Ag–15 at% Mg solid solution alloy. After this alloy has been fabricated to the desired shape of the final component, it is heated in air to 500˚C to allow O to diffuse through the metal and react with the Mg, forming MgO dispersoids. (Ag does not oxidize at this temperature, but it does permit O diffusion through its lattice.) (a) Estimate the percent mass change that such an Ag–Mg alloy would undergo as the Mg oxidizes internally. (b) Would you expect the Ag matrix to harden as a result of an increase in dislocation density caused by the volume change of the Mg + O  MgO reaction during the anneal?

9.10. It is possible to generate electricity by converting the kinetic energy of an orbiting spacecraft to electric power using a long wire that cuts Earth's magnetic field lines as it orbits (Sidebar 18.2). Early trials of this concept focused on use of a Cu–Nb metal matrix–metal reinforcing phase wire, but on a mass basis, Al is a better conductor of electricity than is Cu. Since the cost of boosting the wire into orbit is quite high, a high-strength Al matrix composite would be a potentially superior material for this application. Examine binary-phase diagrams and recommend a ductile metallic element that could be used for the reinforcing phase in a P/M deformation-processed metal–metal composite with a pure Al matrix. Explain why the choice you recommended is the best option.

10.1. In Fig. 10.3 the thermal conductivity of Na is shown as 92 W/mK at 100˚C. In Table 10.1, the thermal conductivity of Na is given as 140 W/mK at room temperature. Briefly explain why Na’s thermal conductivity changes so much over this temperature range of approximately 75˚C.

10.2. (a) Assume that a neutron traveling at 3.00(103) km/s strikes the nucleus of a motionless 11Na23 atom in a reactor core. The collision causes the neutron to recoil elastically, and it travels backward along exactly the same path it traveled as it approached the atom. Calculate the velocity of the neutron after the collision. (b) Perform the same calculation for a 3.00(103)-km/s neutron striking a 3Li7 atom nucleus. Based on your answers from these two calculations, which metal would perform better for use as a coolant in a LMFBR, where high neutron velocity is preferred?

10.3. Na has been observed to slip on three different slip planes: {110}, {211}, and {321}. Metals usually slip on the slip plane that has the highest atomic planar density (i.e., the largest number of atom nuclei per unit area). Calculate the planar density of atoms on the (110), (211), and (321) planes of Na.

10.4. At room temperature, Rb metal is very near its melting temperature. Would you expect a specimen of Rb metal held in inert gas at room temperature for several years to eventually experience so much grain growth that it would become a single crystal?  Explain your answer.

10.5. The density of Fr is unknown. Estimate Fr’s density assuming that the lanthanide contraction (Sec. 1.6) gives Fr the same atomic radius as Cs.

10.6. Assume that you are employed by a large company that has recently purchased a smaller company. The smaller company has an inventory of four train tank cars full of NaK eutectic alloy. Your company has no use for NaK, and your supervisor wants to put these tank cars back into service hauling other cargo. She assigns you the task of brainstorming five ideas for obtaining some value from the NaK. Develop a list of five possible industrial, military, or consumer products uses for this large quantity of NaK.

10.7. Li2O has a cF12 (Sidebar 1.1) CaF2 type of structure. Li2O has a lattice parameter of 0.4628 nm and a melting temperature of 1570˚C. Calculate whether Li2O will sink or float on liquid Li. You may neglect thermal expansion effects and the volume change that occurs when metallic Li melts.

The Pearson designation cF12 indicates that this crystal structure is cubic and has 12 atoms per unit cell. The masses in grams of O and Li atoms can be calculated:

MassLiatom=6.939gmol6.023(1023)atomsmol=1.152(10−23)gatom

MassOatom=15.999gmol6.023(1023)atomsmol=2.656(10−23)gatom

Using the masses of the atoms and the given information about the Li2O unit cell, the density of Li2O can be calculated:

Li2Odensity=8(1.152(10−23)g)+4(2.656(10−23)g)(0.4628nm)3=2.00gcm3

Since the density of Li metal (0.54 g/cm3) is much lower than the density of Li2O, the oxide will sink in a pool of liquid Li metal.

10.8. An ion rocket using Cs as the fuel has been designed to eject a stream of electrons from an electron gun during operation. Because of their low mass, the electrons provide little thrust. Why, then, have the engineers planned for the added complexity and weight associated with the electron gun?

10.9. A martensitic transformation occurs in Li by distortion of the BCC unit cell, transforming the (011)BCC plane into a close-packed plane. (a)  Sketch the atom positions on the Li (011) plane and label all <111> directions that lie in this plane. (b) Assuming an atomic radius of 0.152 nm, calculate the planar atomic densities of the (011)BCC plane and of the closest-packed plane that replaces it.

10.10. Na is the least expensive of all metals on a cost per volume basis. Calculate the cost in dollars per liter for Na, Fe, Pb, Al, Cu, and Zn.

11.1. As described in Sec. 11.3.2.2, the CRSS values for Be and its alloys vary greatly among the basal, prism, and pyramidal slip planes. It is desired to perform a room-temperature single-crystal compression test that will prevent slip on the basal and prism planes and activate slip on the 1122 pyramid plane of a Be alloy. (a) Determine what crystallographic direction(s) would need to be parallel to the direction of the compressive force in this test to achieve this goal. (b)  If the following are the CRSS values for the Be alloy at room temperature, calculate the maximum alignment error (in degrees) that can be tolerated in aligning the single crystal in the desired orientation to assure that slip will occur on the pyramidal plane.

| Be Slip System | CRSS (MPa) |
| --- | --- |
| Basal (0001)1120> | 1.6 |
| Prism 10101120> | 14 |
| Pyramid 11221123> | 2100 |

11.2. The Stroh relation predicts that Be strength is controlled by basal plane cleavage failure.

sN=4gmcosqpDtsIn this equation N is the applied normal stress, s the effective resolved shear stress,  the surface energy,  the angle between the basal plane and the tensile axis, and D the dislocation slip distance (taken to be the grain size in polycrystalline specimens or specimen diameter in single crystals). Calculate the N value for single crystal Be cylinders with diameters of 1mm, 10 m, and 100 nm, and 1 nm. Assume that  is 45˚ in all cases. The shear modulus () of Be is 16.4 GPa on the basal plane. Discuss the reasonableness of your calculated values.

11.3. The bending moment, I, for a solid beam with a square cross section can be used to calculate the elastic deflection (x) at the end of that beam by the following equations:

Dx=−PL33EII=b412

(a) Assume that a beam of solid Mg with a cross section of 0.050 m x 0.050 m (i.e., b = 0.050 m) is loaded as shown in Fig. 11.15. Calculate the elastic deflection (x) in meters at the top end of the beam caused by applying a load, P, of 25.0 N. The load is attached to the very end of the beam, 1.5 m (L) above the floor.

(b) A steel beam of square cross section is positioned beside the Mg beam.  The steel beam has the same length and mass as the Mg beam. For the steel beam to have the same mass as the Mg beam, its cross-section dimension, b, must be smaller than 0.050 m. Calculate the elastic deflection in millimeters at the top end of the steel beam when a load, P, of 25.0 N is applied. The elastic modulus of steel is 207 GPa.

11.4. A person puts a thin latex surgical glove on one hand and leaves the other hand bare. He then takes two chunks of Ca metal and holds one lump on the palm of each hand for several minutes. He notices that as time goes by, the metal on the bare hand begins to feel warmer than the metal on the gloved hand. The two lumps of metal were both at room temperature before he picked them up; explain why one piece feels warmer after he has held it for awhile.

11.5. The manager of an x-ray tube manufacturing operation wants to explore the possibility of reducing manufacturing costs by replacing Be with Mg as the window on their x-ray tubes. He has calculated that a pure Mg window would need to be twice as thick as a pure Be window to bear the stress of the 1 atm pressure differential across the window. The x-ray energy of interest is 8.04 keV, and at this energy the absorption cross sections are 1.01 cm2/g for Be and 40.9 cm2/g for Mg. Calculate the ratio of transmission (percent x-rays transmitted by Be/percent x -rays transmitted by Mg) for the case where the Be window thickness is 0.020 cm, and state whether the Mg replacement idea would be a feasible cost-saving measure.

11.6. Use Table 11.3 and Fig. 11.13 to determine the constant, A, for steady state creep of Mg alloy MRI153 at 135˚C under an applied stress of 85 MPa.

11.7. Mg has three naturally occurring stable isotopes; their atomic weights and relative abundances in Mg are Mg24 (at. wt. 23.985, 78.99% abundant), Mg25 (at. wt. 24.986, 10.00% abundant), and Mg26 (at. wt. 25.983, 11.01% abundant). The isotopic content can be altered by using isotope enrichment methods (Sec. 24.4.2.1). (a) The density of naturally occurring Mg is 1738 kg/m3. Calculate the density of Mg after its isotopic composition is altered to 96.5 at% Mg24, 1.9 at% Mg25, and the balance Mg26. (b) The isotopic enrichment process is very expensive. Would the improved density calculated in part (a) justify the expense of the isotopic enrichment process?

11.8. A Mg sacrificial anode is connected electrically to a buried steel gasoline storage tank. The anode lost 1.2 kg of Mg metal in a 180-day period. Calculate the average current (in amperes) that flowed through the wire connecting the Mg anode to the tank during this time period.

11.9. Mg alloys have improved creep resistance when Ca and Sr additions are made to form CaAl2 and SrAl2 intermetallics at the grain boundaries. Ba metal forms a similar BaAl2 intermetallic. Comment on the reason(s) that Ba has not been used to improve creep performance in Mg alloys.

11.10. Most high-voltage power transmission cables are constructed of pure Al metal. Pure Al is quite weak, so the Al is encased in a stainless steel sleeve for strength. Write a brief assessment of the feasibility of replacing Al with Ca in these cables. Your assessment should address the issues of cost, electrical conductivity, weight, ease of manufacturing the metals into cable, and corrosion resistance.

11.11. A 5.000-g quantity of 88Ra226 isotope is present in the form of RaCl2 sealed inside an evacuated quartz ampoule. The total internal volume of the ampoule is 3.00 cm3, some of which is occupied by the RaCl2 (density = 4.91 g/cm3). Calculate how long it will take this material to produce enough gaseous 86Rn222 to reach 1 atm of Rn gas pressure inside the ampoule.

88Ra226  86Rn222 + 2He4 (t1/2 = 1600 years)

86Rn222  84Po218 + 2He4 (t1/2 = 3.82 days)

84Po218 is a solid.

12.1. The ability of Ti to absorb its own oxide allows it to be diffusion bonded more easily than other metals. However, diffusion bonding drives the O formerly present at the metal surfaces into the bulk metal, raising its O content. This carries the risk of degrading the metal's ductility and fracture toughness. (a) Two 0.90-mm-thick pieces of Ti sheet (O content = 1500 wt ppm) are diffusion bonded by stacking one plate on top of the other. Calculate the increase in bulk O content (ppm by weight) within the metal if their original oxide scale was a 5.0(101)-nm-thick layer of TiO2 (Fig. PS12.1). Assume that the O initially present in all four oxide layers becomes distributed uniformly throughout the sheets by the diffusion bonding. (b) Use Fig. 12.3b to estimate the reduction in ductility that would result from this change in O content.

12.2. A 12.0-m-long wire is needed to hold a tensile load of 5200 N in a corrosive hot-brine environment. Two materials are being considered for this task. One is cold-drawn 304 austenitic stainless steel (density = 8.0 g/cm3, y = 760 MPa); the other is Ti–6% Al–4% V in the quenched and aged condition (density = 4.43 g/cm3, y = 1100 MPa). Both metals have satisfactory corrosion performance for long-term service in this environment. The 304 stainless steel costs $2.80/kg when fabricated into wire; calculate the final fabricated cost the Ti–6% Al–4% V wire must have if it is to have a cost equal to that of the stainless steel wire. Assume a safety factor of 2.0.

12.3. Hf (containing about 4% Zr) is produced as a by-product of the separation of Zr and Hf chlorides. The amount of Hf available exceeds current demand for the metal. Write a paragraph describing a possible new use for Hf metal. Your description should indicate what property or properties of Hf would be useful in your proposed application, and it should also describe at least one potential problem that would need to be overcome to market your concept successfully.

12.4. Sidebar 12.2 describes a building used to weld and heat treat large sections of Ti alloy to assemble submarine hulls. The interior atmosphere of this building was filled with inert gas to avoid contaminating the Ti in the weld zone. Various other industrial processes use inert gases for similar reasons (although not on such a large scale); the gases used for these other processes include N2, CO2, Ar, and He. Make an assessment of these four candidate inert gases for use in the Ti submarine assembly building using the following criteria: cost, reactivity with Ti, availability in large quantities, and any other factor(s) you consider to be relevant. Based on your assessment, select one of these gases for this application.

12.5. Make a Darken and Gurry analysis to predict whether Zr will have extensive solid solubility in Ti, and vice versa. Compare the result of your analysis with a published Ti–Zr binary phase diagram; was your prediction correct?

12.6. Friction stir welding (FSW) is often used to join aluminum plates. Assume that you have been asked to predict how well friction stir welding would work to join Zircaloy-4 plates. Assemble a list of advantages and special problems that Zircaloy-4 would experience with this joining method and recommend two possible tool materials for Zr FSW.

12.7. A plate of Ti–13% V–11% Cr–3% Al alloy was initially solutionized above the beta transus temperature to achieve a single-phase solid solution, then cooled rapidly enough to room temperature to retain an all-beta structure. Figure 12.11 suggests that a similar degree of aging would be achieved in this material by holding it for a day at 500˚C or alternatively, by holding it for a day at 600˚C. A veteran engineer familiar with Ti processing recommends the 500˚ C aging as the better choice. Give two reasons why the lower-temperature aging treatment would be preferable.

12.8. A thick plate of Ti–6% Al–4% V has an equiaxed grain structure. The plate contains an edge crack 1.2 mm deep. When the plate is loaded in tension perpendicular to the plane of the edge crack, the plate fractures at a tensile stress of 390 MPa. Calculate the KIC value for this specimen and state any assumptions you made in determining this value.

12.9. Most of the elements in the periodic table have been alloyed with Zr to determine whether they might be useful  or  stabilizers, but Tc has not been included in these studies, due to its radioactivity, high cost, and limited availability. Based on Zr's behavior with other transition metals, predict whether Tc would act as an  stabilizer, a  stabilizer, or neither in Zr. Justify your conclusion.

12.10. Many lunar rocks have been found to have higher concentrations of Ti than those in terrestrial rocks. However, the moon lacks most of the geological and weathering processes that occurred on Earth to produce rutile sands, so most of the Ti is in silicate-based rocks in compounds containing Fe and other metallic elements. Prepare a one- to two-paragraph concept narrative and/or annotated drawing describing a method to produce Ti metal for use in building structures on the surface of the moon. Describe any special advantages or problems such an operation would have in comparison to Ti production on Earth. Do not be overly concerned with the cost of your proposed concept.

13.1. Estimate the room-temperature strain rate sensitivity, m, for Ta by comparing the ultimate compressive strength of Ta tested at a strain rate of 10-3 s-1 (450 MPa) with that of the test shown in Fig. 13.10.

m=dlnsdlne·

13.2. Suggest a process for producing a microstructure like that shown in Fig. 13.3 for V3Ga superconducting filaments in a Cu or Cu alloy matrix. Make a list of factors that would need to be determined and/or tests that would need to be performed to confirm the feasibility of your proposed process.

13.3. Compare the yield strength of the purest Nb shown in Fig. 13.6 with the yield strength of high-purity Re (Sec. 15.5). Both these elements are strongly bonded refractory metals; suggest one or more possible reasons for the large disparity in their tensile yield strengths.

13.4. (a) Use a ceramic materials properties resource to find two oxides that have a coefficient of thermal expansion approximately the same as that of Ta metal over the temperature range 20 to 1500˚C. (b) Propose a method to apply a thin, adherent layer of these oxides to the surface of a piece of Ta. (c) Discuss possible problems that could arise if Ta coated with these oxides is put into service as a thrust vectoring component that is exposed directly to the exhaust blast of a jet engine.

13.5. V and Nb are frequently used as alloying additions to steel, but Ta is seldom added to steel. Why is Ta so rarely used in steel?

13.6.  A Ta capacitor is proposed for use in a device that will be placed in a waterproof container inside a nuclear reactor core near the fuel rods. Describe at least two possible threats to the proper function of this capacitor in that environment. Describe steps that could be taken to minimize or avoid these problems.

13.7. The Nb–O alloys whose room-temperature tensile test results are plotted in Fig. 13.6 show O contents as high as 11,900 atomic ppm, which appears to be much higher than the maximum solubility of O in Nb at room temperature that one can estimate by extrapolating the O curve in Fig. 13.4. Would you conclude that there are errors in these data, or is there another possible explanation? If so, describe it.

13.8. Estimate the cost of the Ta metal in the capacitor shown in Fig. 13.8. State any assumptions made in your computations.

13.9. Figure 13.4 shows about 32 at% equilibrium solubility for H in Nb at 500˚C. If H dissolves only in the tetrahedral voids of Nb, and a maximum of only one H atom can occupy a void, what fraction of the tetrahedral voids are occupied by H when the H content is 32 at%?

13.10. Assuming the hard-sphere model for atoms, calculate the maximum diameters of interstitial impurity atoms that can fit in the octahedral and tetrahedral voids of Nb (atomic radius = 0.143 nm) without displacing the Nb atoms.

14.1. Write a short paragraph criticizing the following proposal to produce wheels for high-performance automobiles: “Alloy steel will be quenched and heat treated to produce tempered martensite for high strength and good toughness. The wheels will then be pack coated to deposit a protective coating of Cr prior to sale.” Your paragraph should include suggested alternatives to improve the product.

14.2. If Mo at 1000˚C loses 1.5 g/cm2·h due to formation of volatile oxide during exposure to air, estimate the time needed for a solid sphere of Mo 10 cm in diameter to disappear completely when held in air at 1000˚C.

14.3. Is the mass loss rate for W metal exposed at 1000˚C to air greater than the 1.5 g/cm2·h loss rate of Mo at 1000˚C? Show calculations to support your answer.

14.4. Use Fig. 14.11 to determine the critical resolved shear stress for slip at 200 K in W on the {110}<111> slip system (a) with a tensile orientation of [001] (i.e., the lower curve on the figure), and (b) with a tensile axis orientation of <111> (i.e., the middle curve on the figure).

14.5. Highly cold-worked Mo–Re alloys have been reported to have a dislocation density of about 1014 cm-2. For convenience in calculation, assume that dislocations at this density are lying parallel to one another and are all equally spaced from their nearest-neighbor dislocations. Calculate the distance between nearest-neighbor dislocations.

14.6. Doping W with KAlSi3O8 reduces grain growth and creep rates. Could KAlSi3O8 additions be used to improve creep performance in Ti? Justify your answer.

14.7. The shot put is a track and field event in which a solid metal ball is thrust forcefully upward and outward by the athlete, the goal being to achieve a throw of maximum distance. Some athletes complain that the diameter of a gray cast iron ball weighing the regulation 7.27 kg is too large to control comfortably in the hand. (a) Calculate the diameters of 7.27-kg balls made of cast iron and of W. (b) Calculate the relative costs of the cast iron versus W balls. State all assumptions made in your calculations.

14.8. The load-bearing internal framework of most large buildings is fabricated from I-beams made of hot-rolled low-carbon steel with a pearlitic microstructure. Write a one-page commentary on the advantages and disadvantages associated with replacing these steel beams with pure cold-rolled Mo. Your analysis should address the following issues: the relative yield strengths of the two metals, the relative costs of structures having equal strengths, the performance of these two alternatives in a major building fire, the weldability of the two materials in the field, and the anticipated corrosion performance of the two metals.

14.9. Just above its melting point, the density of liquid Cr is 6.0 g/cm3. Heating a bar of solid Cr lengthens it to 1.0248 times its room temperature length just before it melts. Use this information to estimate the percent volume contraction of Cr upon freezing.

14.10. The resistivity of a nichrome wire is 1.50(10-6) ·m. The emission of energy by radiation from a perfect blackbody is expressed by the equation E=ST4, where E is the total energy emitted at all wavelengths, S the Stefan constant (5.669 x 10-5 erg·cm-2·K-4·s-1), and T is the temperature of the emitting material (K). Calculate the DC voltage needed to maintain a straight, 1.00-m-long, cylindrical nichrome wire (diameter = 0.100 cm) at 950˚C in a vacuum. Assume that the wire acts as a perfect blackbody emitter, and neglect thermal conduction through the wire ends.

14.11. Most dies for die-casting Zn–Al alloys (Sec. 19.2.3.3) are made of steel; however, prolonged use of the dies gradually erodes the steel because there is some reaction between Fe and liquid Zn. Prepare a one-page assessment of the feasibility of replacing steel with Mo or Mo alloys to make dies for die-casting Zn–Al alloys. Your assessment should address issues of compatibility of the steel and Mo with liquid Zn, the thermal conductivity and hot tensile strengths and fatigue strengths of Mo alloys and steel die alloys at the temperatures involved with this operation, cost, and ease of fabrication to achieve the needed die geometries.

15.1. The solidification and cooling of pure Mn is a complex sequence of phase changes and volume changes. (a) Assume that a specimen of liquid Mn has a volume of 1000.0 cm3 at the melting temperature of 1244˚C. Use the following information about Mn allotropes to construct a plot of volume (y-axis) versus temperature (x-axis) for this specimen as it cools to 20˚C. Label on your plot the final value of specimen volume at 20˚C.

15.2. In section 15.5 we state that “Re is ductile over a much wider temperature range (0 to 3453 K) than any other solid.” Determine what material is in second place behind pure Re, and state the approximate temperature range of its ductility. Exclude Re-containing alloys from your search.

15.3. (a) Estimate how many atoms would emit a -particle each second in 1 g of Tc99 (t1/2 = 210,000 years).  (b) Calculate how many atoms would emit a -particle each second in 1 g of Re.

15.4. Mild steel immersed in water containing small concentrations of the pertechnetate ion (TcO4-) corrodes at a much lower rate than steel immersed in ordinary water. Write a short paragraph presenting a possible explanation of the mechanism(s) whereby this ion reduces corrosion in steel (see Cartledge, Journal of American Chemical Society, 77, 2658 (1955).

15.5. The brittleness of pure Mn renders it unfit for use as a structural material; however, many other uses are possible. Consider the properties of Mn, and write a paragraph describing two possible uses for pure Mn that are not among the uses described in this chapter.

15.6. Section 15.4.2.2 states that Tc might be a suitable substitute for Re in Ni superalloys, but no evidence to support this claim is presented. Write a description (about 200 words) of an experiment to measure how well Tc would perform if used in this manner.

15.7. If Mn nodules from the deep ocean floor have a composition of 30% Mn, 24% Fe, 1% Ni, 0.5% Cu, and 0.5% Co, calculate the value in dollars of the metal content of 1 ton of nodules.

15.8. Ni superalloys often contain 1 to 2 at% Re. The Re segregates primarily to the  solid-solution matrix, forming clusters that are about 1 nm in diameter. Calculate the number of Re atoms needed to form a 1-nm cluster.

15.9. In Sec. 15.5.2.1 the statement appears that Re–W thermocouples can be used at temperatures as high as 2200˚C. The melting points of Re and W are 3180 and 3422˚C respectively. Why is the use of Re–W thermocouples limited to temperatures about 1000 ˚C lower than the lower of these two melting points?

15.10. Pure Mn can be electroplated quite well onto steel, and it forms an adherent coating on the steel. The standard electrode potential of Mn is more electropositive than Zn, and hence the Mn can perform the function of sacrificial anode more effectively than Zn in terms of electrode potential. In addition, electrolytic Mn prices are usually lower than the price of Zn. However, Zn coating on steel is widely used, whereas Mn-coated steel has no market. Describe two possible reasons why Zn is preferred to Mn for this use.

16.1. The density of Co metal decreases 0.15% when the metal transforms from  to . In theory, the HCP and FCC crystal structures are both densest-packed structures with exactly equal 74% packing efficiency. Explain how this small density change can occur in the HCP  FCC transformation.

16.2. A piece of high-purity Ni exposed to pure O2 at 750˚C is found to gain 1.00 g in mass during a specified time period. At what temperature would an identical piece of Ni gain 2.00 g in mass during the same time in the same atmosphere?

16.3. Large efficiency gains could be achieved in jet engines if the operating temperature of the combustion zone could be raised to, say, 1500˚C. However, the solidus temperature of Ni superalloys is about 1300˚C. Propose two alternative materials that could possibly be used at 1500˚C and briefly list advantages and problems with each of your proposed materials for this use.

16.4. An eutectic composition Ni–Cr alloy is plasma-sprayed onto a cold substrate. This process cools the liquid metal too rapidly to achieve the equilibrium microstructure predicted by the phase diagram. The as-sprayed Ni–Cr metal is then vacuum annealed at 1000˚C for one month, followed by a water quench. (a) Make a sketch of the microstructure you would expect to see in this material after the quench, and label the phase(s) present in the microstructure. (b) Make an educated guess as to whether the quenched material would be brittle, have low ductility, or have high ductility. Explain the reasoning behind your ductility prediction.

16.5. What elements and/or compounds would be present at equilibrium at 1000˚C in a material comprised of 60 at% C, 20 at% Co, 20 at% W?

16.6. (a) Calculate the inherent material value the U.S. 5-cent coin would have if it were made of pure Ni. This coin is 21.21 mm in diameter and 1.95 mm thick. (b) The U.S. 5-cent piece is actually an alloy of 75 wt% Cu–25 wt% Ni. Calculate the inherent material value of the 75 wt% Cu–25 wt% Ni coin.

16.7. The microstructure of Inconel 625 alloy shown in Fig. 16.13 contains many carbide particles. Are these Ni carbides? If so, predict their chemical formula(s). If not, what element(s) would be present in these carbides?

16.8. Calculate the increase in density that results when 3.0% Re is dissolved as a solid solution in Ni. You may neglect strain effects from the larger Re atoms and assume that they substitute for Ni atoms without changing the lattice parameter (0.354 nm).

16.9. Assume that an x-ray diffraction pattern is taken from two specimens of pure Ni. The two specimens are identical except that one contains numerous twins, while the other is untwinned. Would the XRD patterns show a larger number of diffraction peaks for the specimen containing the twins? Explain the reasoning behind your answer.

16.10. Stainless steel and Ni-base alloys are often used in nuclear fission reactor core structures because of their good corrosion resistance and mechanical properties. However, Ni intended for use in reactor alloys is given an additional processing step to remove Co. Explain why Co needs to be removed and suggest a method that could be employed to remove Co from Ni.

17.1. Use the Rice–Thomson criterion to estimate the maximum value for free surface energy in Os, given that the shear modulus, , is 234 GPa and the lattice parameters are a = 0.273 nm and c = 0.432 nm. State any assumptions used in your estimations.

17.2. Ru and Rh have about the same terrestrial abundance and similar quantities are produced each year, but the price of Rh is much higher than the price of Ru. Write a short paragraph to present a possible explanation for this price disparity.

17.3. Erosion and surface roughening are common problems in electrical switches used in high-voltage, high-amperage circuits. This damage is caused by arcing when the switch opens and closes (Fig. 18.22). (a) Consider the properties of the six pure PGMs and recommend one of them as best suited for use as the contact surface in such switches. (b) Write a paragraph that describes advantages and disadvantages of using a PGM alloy for the switch contact rather than one of the pure metals.

17.4. Os's odd combination of properties make it a metal with few applications. Brainstorm five new ideas to expand the market of Os, and write a one or two sentence summary of each idea.

17.5. Assume that an alloy of Ir–0.3% W is used to encapsulate a Pu238O2 heat source for a thermoelectric power source to be used on a deep-space mission. The Ir alloy is present as a 0.8-mm-thick sheet welded around the oxide. The decay heat of the Pu keeps this assembly at a temperature of 1000˚C. Calculate how long the assembly could sit in air before 10% of the Ir alloy is lost.

17.6. A chemical process industry reaction requires a pure Pd catalyst in the form of a 1-mm-thick sheet with 90% porosity (effective density = 1.2 g/cm3). Describe a processing method that could be used to produce this material.

17.7. Pd and Au have complete solid solubility at all temperatures and compositions. Adding 20 wt% Pd to Au increases the solidus temperature from 1064˚C to 1250˚C, which is hot enough to allow an Al2O3-based ceramic veneer to be fired at 1200˚C around an Au–20% Pd alloy stump for a dental implant. The coefficient of thermal expansion of this ceramic is 7.3 x 10-6 ˚C-1. (a) Use the rule of mixtures to estimate the coefficient of thermal expansion of the Au–20% Pd alloy. (b) The Au–Pd stump is a solid, 3mm diameter cylinder with a roughened surface to improve the adherence of the ceramic veneer. Assuming the ceramic-metal interface remains well bonded during cooling to room temperature, will the ceramic veneer have a residual tensile or compressive hoop stress near the ceramic-metal interface?

17.8. Pd is often used as a diffusion membrane (called a “septum”) to separate H2 from impurities, producing high-purity H2. H diffuses rapidly through the septum, but the impurity gases diffuse much more slowly. A typical Pd septum is Pd–25% Ag alloy in 80.0-m-thick sheet. The diffusion coefficient for H in this alloy is 3.0 x 10-6 cm2/s at 400˚C. Calculate the H2 throughput in grams per hour of a septum of 0.10-m2 area if steady-state diffusion occurs at 400˚C and the H concentration in the Pd at the impure gas surface is 1.8 kg/m3 and the H concentration in the Pd at the pure gas surface is 0.40 kg/m3.

17.9. Experimental Pt catalysts for fuel cell use have been created with an average Pt particle size of only 2.0 nm. Calculate the total surface area of 1.0 g of this nanoparticulate Pt and state any assumptions made to obtain your answer.

18.1. (a) Calculate the theoretical shear strength of a pure Cu single crystal using the equation  = G/30, where G is the shear modulus.  (b) Gertsman, et al. (1994) developed a Hall–Petch expression for pure Cu: y = 92 + 399d-0.5, where stress units are in megapascal and length units are in . Use the Gertsman equation to estimate the grain size that would be required in a pure Cu sample to produce the yield strength expected for a material with the G/30 shear strength determined in part (a).

18.2. (a) Perform a Darken–Gurry prediction on whether each of the following elements will have extensive (>5 at%) solid solubility in Ag: Er, Na Mg, Ti, and V. For each element, state whether it meets the size and electronegativity criteria. (b) Find an equilibrium binary phase diagram for each of these five systems and state whether your predictions in part (a) were correct.

18.3. A solid cylindrical rod of W is 10.0 cm long and 0.707 cm in diameter. A 10.0-cm long cylindrical sleeve of Ag is fitted tightly around the W; the Ag tube has an inside diameter of 0.707 cm and an outside diameter of 1.00 cm. The Ag metal was cast around the W rod in a vacuum, so a strong metallic bond exists at the interface between the two metals. No residual stresses exist in either metal at 500 K. The metals are then

quenched from 500 K to 77 K. The bond at the W–Ag interface remained intact during this quench. (a) Predict whether the thermal stresses induced by quenching will cause the Ag to reach its yield point or to fail by fracture. (b) Predict whether the thermal stresses induced by quenching will cause the W to reach its yield point or to fail by fracture.

18.4. To estimate the dislocation density that would be needed in pure Cu to raise the ultimate tensile strength to 450 MPa, the value considered to be “full hardness” for cold-worked Cu, use the equation Gb1/2, where  is the yield stress (MPa),  a dimensionless constant ≈ 0.5, G the shear modulus (MPa); b the length of the Burgers vector (cm); and  the dislocation density (cm-2).

18.5. During World War II, military production made Cu a scarce commodity in the United States. When the calutrons for U isotopic enrichment were constructed for atomic bomb production, an enormous amount of wire was needed for construction, and planners were concerned that using so much Cu would cause shortages for other military production. Therefore, the project was constructed using 15,000 tons of Ag wire fabricated from the U.S. monetary Ag reserves held to back the value of the dollar. Calculate the diameter of a Ag wire that would have the same electrical resistance as a 3.00-mm-diameter Cu wire.

18.6. When pure Ag becomes corroded with Ag2O or Ag2S films, it can be cleaned simply by heating it in air to 300˚C or hotter, which decomposes the films to Ag metal and O2 or SO2 gas. However, when this procedure is used to attempt to clean corroded sterling silverware, the corrosion of the metal actually worsens. Explain why this method fails to remove the corrosion from the silverware.

18.7. The binary equilibrium phase diagrams of Au with other metallic elements contain an unusually large number of intermetallic compounds. Give a one-sentence explanation of why Au forms intermetallic compounds with so many other metals.

18.8. In Au refining facilities, the used cotton gloves worn by the workers who handle Au bullion bars are reprocessed to recover the traces of Au that accumulate between the fibers of the cotton cloth. Design a process with cotton gloves containing traces of Au as the input material and pure Au as the output material. Describe any by-product outputs produced by your process.

18.9. The great ductility of Ag and Au allow them to be drawn into fine wire that can be woven into cloth. Assume that a noted fashion designer learns that Au and Ag cloth is available. He wants to explore the possibilities of marketing Au and Ag clothing to wealthy clients as the “ultimate fashion statement”. Further assume that he asks your technical opinion about the feasibility of this marketing concept. Write a one-page assessment of the possible drawbacks to such a consumer product.

18.10. Studies on single crystals of Cu–1.3 at% Mn solid solution alloy produced the following data for dislocation density () and shear stress () for slip on the {110} slip planes:

 (m-2) 	(MPa)

1.96 x 1012	12

4.84 x 1012	15.5

19.4 x 1012	21

61.6 x 1012	36.5

151 x 1012	53

Use these data and the expression Gb√ , to estimate the critical resolved shear stress () for slip in this Cu–Mn alloy. The Burgers vector length (b) is 0.256 nm,  is 0.32, and the shear modulus (G) is 42 GPa for this composition.

19.1. (a) Criticize the following proposal to prepare high-strength gate latches for a security fence. (b) Describe one or more changes to the proposed process to improve the performance of the 4340 steel latches, and explain how your change(s) will improve performance.

The 4340 steel latches are received in furnace-cooled, pearlitic condition from the fabricator. The latches will be degreased, pickled, coated with a ZnCl2·3NH4Cl flux, and hot-dip galvanized. The parts will then be austenitized at 1000˚C for 20 minutes, water quenched, and tempered for one hour at 350˚C. This will produce a latch that is strong and tough to resist mechanical damage with good corrosion resistance to avoid rust in its outdoor service environment.

19.2. A pure Zn single crystal is deformed by easy glide at -50˚C, as described in Sidebar 19.1. Use the information given in Sidebar 19.1 and Fig. 19.2 to predict how long it will take the deformed crystal's shear stress to decrease to 300 kPa if it is warmed to -10˚C immediately after deformation and held at that temperature.

19.3. (a) Describe a processing method that could be used to prepare an alloy that is 60 wt% Ag–40 wt% Hg. Your instructions should be sufficiently detailed that a technician could produce the alloy without having to ask you for additional information or directions. (b) Predict whether this alloy will be single-phase or two-phase.

19.4. The hot-dip galvanizing process is often used to apply a protective Zn coating to the surface of steel. It is also possible to apply a Zn coating to steel by thermal spray (Sec. 8.7.3), which fires small droplets of liquid Zn onto the steel surface, where they cool rapidly to form a pure Zn coating. This method has the advantage that it can be used on steel structures too large to fit into hot-dip tanks. Describe two possible disadvantages to applying Zn onto steel by thermal spray.

19.5. A maximum in yield stress is observed in single-crystal Cd for slip on the 1122<1123> slip system (Fig. 19.11). No maximum in seen in the yield stress of polycrystalline Cd; it decreases steadily as the temperature rises. Briefly explain why no yield stress maximum is present in polycrystalline Cd.

19.6. Assume that you are given a precisely machined cube of single crystal Zn. Each edge of the cube is 20.00 mm ± 0.01 mm long. You are told that one of the edges is parallel to the [0001] direction, but you don't know which edge it is. Describe a method to determine which edges are parallel to the [0001] using only a micrometer and the items available in an ordinary household kitchen.

19.7. The argument has been made that the risks of Cd toxicity outweigh the benefits of its use and that all Cd use should be banned. If a total ban were placed on Cd use, Cd production would continue because Zn ores contain roughly 2 g of Cd for every kilogram of Zn. Devise a plan to deal with this “unwanted” Cd production. Your plan should prevent the Cd from being dispersed into the biosphere, where it could potentially harm animals or people, and it should do so at the lowest possible cost. Describe your plan in one paragraph.

19.8. Calculate which metal costs less on a dollars per cubic centimeter basis, Zn–4 wt% Al die-casting alloy or commercial purity Al. Base your calculation solely on raw material costs, ignoring all other costs.

19.9. Consider the attributes of superplastically formed Zn–22% Al alloy and describe three familiar items that could be produced with this material. Write a brief  description of each of the applications, detailing potential advantages and disadvantages of using this alloy to make the object in question.

19.10. Commercial purity Zn sheet has been widely used as a roofing material for buildings in northern Europe for more than 100 years. However, it is seldom used in other parts of the world. This pattern of use is not just a matter of whim or fashion. Briefly describe a metallurgical reason why Zn sheet would work better for roofing in London than it would in Riyadh.

20.1. An alloy consists of 99.85 wt% Al and 0.15 wt% Zr. (a) Calculate how many Al3Zr dispersoid particles can form per cubic centimeter of metal if each particle is a sphere 40.0 nm in diameter and all the Zr in the alloy resides in the dispersoids. The density of Al3Zr intermetallic compound is 4.11 g/cm3. (b) Repeat the calculation done in part (a) for 100.0-nm-diameter Al3Zr dispersoid particles.

20.2. It is desired to produce a wire 1.00 km in length that will have an electrical resistance of 10.0 . (a) Using the data in Fig. 20.1, calculate the cost of the metal (in dollars) to produce such a wire if it is made from pure Al.  (b) Using the data in Fig. 18.1, repeat the calculation performed in part (a) to determine the cost of the wire if it is made of Cu.

20.3. Calculate the mass of Al that must be deposited onto a 10-m diameter telescope mirror (Sidebar 20.2) to produce a 100.0-nm-thick coating. State any assumptions made regarding the mirror and the Al coating.

20.4. Use Fig. 20.9 to specify a process that will convert 1100 Al rod from the H18 condition to the H24 condition.

20.5. Use Fig. 20.10 to develop a mathematical expression that will predict the yield strength y) of an Al–4.5% Mg solid solution alloy as a function of the amount of its true strain induced by rolling ().

20.6. It is desired to produce an aging heat treatment for Al 2014 that will achieve y ≥ 400 MPa and tensile elongation of 10% or more. Since there is a cost associated with each hour of furnace time spent heat treating the metal, it is desired to keep the aging treatment as brief as possible consistent with achieving these mechanical properties. Specify a heat treatment that will allow the metal to meet these performance specifications at minimum cost.

20.7. (a) Use Fig. 20.18 to calculate the minimum angle between the normal vectors to the Al {111} slip planes and the rod axis of the ´ Mg2Si precipitates. (b) If the ´ Mg2Si precipitates have a circular cross-sectional area of 12 nm2 measured perpendicular to their long axis, calculate the effective elliptical cross-sectional area presented to a dislocation gliding on an Al {111} plane as it attempts to shear through the ´ Mg2Si precipitates at the angle determined in part (a). Assume that a ´ Mg2Si precipitate slip plane happens to be coplanar with this ellipse.

20.8. Ga forms a low-melting eutectic with Al at 26.6˚C and 97.9 at% Ga. If a piece of Al is immersed in liquid Ga and the Al oxide layer is damaged (as by scratching), Ga will diffuse along the Al grain boundaries, and the individual grains of Al will separate from one another, producing what is essentially a three-dimensional jigsaw puzzle composed of the individual grains of Al. Assume you are asked to develop this concept into a salable consumer item. The consumer will purchase the dismembered Al grains and attempt to reassemble the original Al block. Since there is some toxicity concern about Ga, it is desired to remove as much Ga as possible from the Al surfaces before the item is sold to the consumer. It is also desired that the Al grains be reasonably large (several millimeters) so the puzzle will not be inordinately difficult to reassemble. Specify a production process to produce such three-dimensional jigsaw puzzles from Al blocks 10 cm x 10 cm x 1 cm.

20.9. Tl undergoes a 3.2% volume increase when it freezes. Liquid metals are usually nanometer-scale crystalline clusters that are incompletely bonded with their neighbors. What crystal structure would you expect to be present within these clusters in liquid Tl? Explain the reasoning behind your answer.

20.10. The ultimate tensile strength of pure In is 3 MPa. Estimate whether a person of ordinary strength could pull a 1.0-cm-diameter pure In tensile test specimen with sufficient force to achieve tensile failure.

20.11. The die–mandrel configurations shown in Figs. 20.20 and 20.21 work well to produce Al seamless tubing. Write one- to three-sentence opinions of how well these same die–mandrel configurations would work to produce seamless tubing from (a) pure Re, (b) pure Mg, and (c) pure Cu.

21.1. It is possible to produce Si containing only one impurity atom per 1.0(1012) Si atoms. If one assumes that the spacing between impurity atoms in such ultrapure Si is uniform, estimate the average spacing between impurity atoms. The unit cell edge length in Si’s cF8 structure is 0.5431 nm.

21.2. Pure -Sn is difficult to fabricate into monolithic, low-porosity specimens. Castings of -Sn that are cooled through the transformation temperature (13˚C) are slow to transform to the  phase, and when they do transform, the large volume increase on transformation typically causes the specimen to break up and crumble into powder. Powdered -Sn does not sinter well at temperatures below 13˚C. Suggest a method that might allow production of a monolithic, low-porosity specimen of -Sn (either single-crystal or polycrystalline) material.

21.3. From the kinetic theory of gases, the number (n) of gas molecules striking a surface at room temperature is expressed by:

n = 3.798(1020)p cm-2s-1

where p = gas pressure in torr (1 atm = 760 torr). (a) If pure O2 gas at a pressure of 1.0 atm is suddenly released into a vacuum chamber containing an atomically clean (100) surface of a single crystal of Pb, how long would it take to form a monolayer of PbO on that surface? State any assumptions used in determining your answer. (b) Compare this result with the finding that O2 does not seriously degrade fatigue lifetimes if the loading frequency is greater than 200 Hz.

21.4. About 80% of all primary and recycled Pb production is used to make Pb–acid batteries. (a) If world automobile and light truck production totals 60 million new vehicles per year, estimate the mass of Pb needed to equip each vehicle with a Pb–acid battery. (b) Estimate the mass of Pb needed to reequip older vehicles with replacement batteries. State all assumptions used in reaching your estimates for parts (a) and (b). (c) If the sum of your answers to parts (a) and (b) does not equal 80% of world primary and recycled Pb production, present a possible explanation for why the numbers differ.

21.5. Ge and Si are transparent to infrared light; most metals are not. Using one to three sentences and a diagram (optional), explain why these two elements are able to transmit infrared light but not visible light.

21.6. Calculate the relative material costs ($/kg) of a eutectic Pb–Sn solder and an Sn–3.7 wt% Ag–0.6% Cu–0.3% Co solder.

21.7. Liquid Sn is used to produce float glass; however, the process requires a relatively large quantity of Sn, which is somewhat expensive. Assess the feasibility of replacing the Sn with Pb, which costs much less. Is this a useful money-saving idea, or would floating glass on molten Pb pose problems not experienced with Sn?

21.8. Thermisters are devices that measure temperature by monitoring the change in electrical resistance in a semiconducting material. (a) If a thermister is to be designed for use over the temperature range 400 to 1000 K, use Fig. 21.2 to determine which of the following materials would be better suited to this task: a 99.99999999% pure Si rod or a 99.99999999% pure Si rod doped with 13 atomic ppm B. Justify your choice. (b) Write a paragraph describing one or more possible problems that could arise from use of Si in a thermister at 1000 K.

21.9. A plate of free-machining steel is hot rolled at 600˚C to reduce its thickness by 25%. The hot rolling causes several large tears in the edge of the plate, and the surface finish became mottled and uneven. Steel normally tolerates hot rolling under these conditions without showing such defects. Explain what went wrong in this case.

21.10. Estimate the electrical resistance of a Sn whisker 2.0 mm long and 2.0 m in diameter.

22.1. Several Bi alloys are used for their low melting temperatures, but none of the commercial alloys contain alkali metals. The alkali metals have even lower melting temperatures than the Bi alloys, and it might seem worthwhile to see if useful fusible alloys could be produced by alloying Bi with group 1 metals. Predict the probability of producing a useful Bi–alkali metal alloy as being either “high” or “low” and justify your prediction.

22.2. Calculate the energy of an -particle emitted by the decay of 84Po210.

22.3. Write a brief statement describing the expected effect of tensile testing a single crystal of Cu immersed in a bath of molten Bi at 300˚C. Will the presence of the Bi significantly alter the mechanical properties of the Cu single crystal? Justify your answer.

22.4. When heated in a vacuum, As does not melt but sublimes into As4 vapor. Briefly explain why As vapor is As4 rather than As, As2, As3, As5, and so on.

22.5. The 1s electrons in Bi orbit the nucleus at 60% the speed of light. Calculate the effective mass of a Bi 1s electron.

22.6. The slip systems for plastic deformation of -Po have not been determined experimentally. (a) Use the basic concept that slip occurs most readily on planes of highest atomic area density in the crystallographic directions of highest atomic linear density to predict whether the primary slip system for -Po will be the {100}, {110}, or {111} planes. Show calculations to justify your answer. (b) Write a one- or two-paragraph description of an experiment that could be performed to test the correctness of your prediction in part (a).

22.7. Write a paragraph describing how the embrittlement of Cu by liquid Bi might be employed to serve a useful purpose.

22.8. If Pb–3 wt% Sb alloy is chill cast so that it solidifies and cools rapidly, its ultimate tensile strength increases from 30 MPa to 52 MPa when stored at room temperature for 30 days after casting. But if the same alloy is cast in a mold where it cools slowly to room temperature, no significant strength improvement is observed 30 days after casting. Write a paragraph to present your interpretation of what is causing the different behavior of these two castings.

22.9. The maximum permissible body burden for Po210 has been set at 6.8(10-12) g. (a) Calculate how many atoms this is. (b) There are about 1014 cells in the body of a typical adult human. What is the ratio of the number of Po atoms calculated in part (a) to the number of cells in the human body?

23.1. The Pillings–Bedworth ratio (P-B ratio) can be used to predict whether the oxide layer that forms on a metal will be protective. The P-B ratio can be calculated as follows:

P−Bratio=AoxideρmetalAmetalρoxide

where Aoxide is the molecular weight of the oxide, Ametal the atomic weight of the metal, oxide the density of the oxide, and metal the density of the metal. If the P-B ratio lies between 1 and 2, the oxide is often protective. If the P-B ratio < 1, the oxide has insufficient volume to cover the metal surface completely, and if the P-B ratio > 2, the oxide may crack and spall off. Calculate the P-B ratios for Sc, Nd, and Lu and comment on how well the P-B ratio matches the actual oxidation protection provided by the oxides of these metals.

23.2. Although the lanthanide metals are quite similar to one another in the chemical compounds they form, variations are sometimes seen across the lanthanide row in the crystal structures of their intermetallic compounds. The cI2 (CsCl-type) intermetallic structure (Fig. 25.3) forms in the following systems: ErIr, HoIr, LuIr, TmIr, and YbIr. However, this crystal structure does not form between Ir and any of the other nine lanthanides. Suggest a possible explanation for this difference in crystal structures.

23.3. Calculate the average drift velocity of electrons traveling through a pure Sm wire that is 150 m long and has a 1.5 V potential between its ends. Assume that the density of conduction electrons in Sm is 9.0(1022) e-1/cm3. Compare your answer to the average drift velocity of electrons traveling through a pure Cu wire [n = 4.23 (1022) e-1/cm3] under the same circumstances.

23.4. Assume you are given 1 kg of each of the 17 pure RE metals and you are assigned the task of producing the best carpenter's hammer possible using only these metals to make the hammer head and handle. Further assume that you have at your disposal a well equipped shop and metallurgical foundry. Write a one-page description of how you would produce this hammer; include in your narrative the reasoning behind the choices you make.

23.5. When small samples of metallic alloys are needed for research, they are often produced by co-melting the pure elements on a chilled Cu substrate with an electric arc. The arcmelting is done inside a closed chamber with a low-pressure Ar gas atmosphere, to avoid contaminating the metal with O and N. This method was found to work well to make 50-g buttons of a PrRu alloy. However, when an attempt was made to arc-melt 50-g buttons of this same Ru alloy by substituting mischmetal for pure Pr, the viewing window used by the technician to see inside the chamber quickly became opaque. Since this made it impossible to continue the arcmelting, the technician then added enough Ar to bring the chamber up to 1 atm pressure and opened the chamber hatch. Moments after opening the hatch, a loud “woof” was heard as a brief flash of fire raced through the chamber, leaving the technician startled but uninjured. What happened to cause this flash fire?

23.6. A scientist giving a lecture made the statement: “Of course, Sc, Y, La, Yb, and Lu are all in a different class, magnetically speaking, from the other rare earth metals.” What is there about these five elements that makes them magnetically different from the other 12?

23.7. On the phase diagram for pure Ce (Fig. 23.8), there are no data for the liquidus line above about 7 GPa. Explain from an engineering perspective why such data are difficult to acquire.

23.8. The ductility of most metals increases with increasing temperature, but for polycrystalline La the increase is quite large and abrupt between 500 and 600 K (see Fig. 23.12). Write a paragraph explaining the probable cause(s) of La’s large increase in ductility at these temperatures.

23.9. Small additions of Sc improve the performance of Al alloys, but the high cost of Sc limits its use. The Al–Sc and Al–Y phase diagrams are quite similar; in each system Al3Sc and Al3Y are the most Al-rich intermetallic compounds. This suggests the possibility that Y might be substituted for Sc to achieve the same benefits in Al alloys at a much lower cost. Predict the likelihood that Y can be substituted successfully for Sc in this application and explain the reasoning behind your prediction.

24.1. Using the isothermal transformation diagram in Fig. 24.6, specify a heat treatment to process a U–0.75% Ti alloy to achieve high hardness. Assume that the prior thermal history of the alloy is unknown and the workpiece to be treated is in the form of a small sheet 1 mm thick. The description of your heat treatment should be sufficiently specific that a technician could follow your instructions without needing to ask additional questions.

24.2. The Voyager 1 spacecraft was launched in 1977 on a mission to the outer planets, and it has since left the solar system. Its electrical power was provided by Pu238O2 thermoelectric generators sealed in Ir–Pt alloy containers. Assume that the spacecraft is intercepted 1.00(106) years in the future by interstellar travelers and analyzed. Estimate what the elemental composition of the PuO2 would be at that time. The decay sequence for Pu238 is: 94Pu238  92U234 + 2He4 (t1/2 = 87.7 years); 92U234  90Th230 + 2He4 (t 1/2 = 2.45 x 105 years); 90Th230  88Ra226 + 2He4 (t 1/2 = 75,400 years); 88Ra226  86Rn222 + 2He4 (t 1/2 = 1600 years); and 86Rn222 decays to 82Pb206 by a series of decays that all have short half-lives.

24.3. The neutron capture cross section and fission behavior (3.9 neutrons/fission event) of Cf251 (t1/2 = 898 years, -decay) are excellent for weapons use. It has been calculated that a carefully designed weapon using this isotope could be made with a critical mass as small as 200 to 300 g. This would allow construction of a “micro-nuke” atomic bomb that would be smaller and lighter than Pu and U atomic bombs. (a) Calculate the size (in cm3) of 250 g of Cf. Is your answer larger or smaller than a golf ball? (b) Write a paragraph describing two possible drawbacks to construction of such a weapon.

24.4. The surface of an object emits electromagnetic radiation whose total energy can be calculated (assuming it acts as a perfect black-body emitter) using the Stefan–Boltzmann relationT4, where  is the total energy radiated at all wavelengths per square centimeter of the object’s surface,  the Stefan constant (5.67 x 10-5 erg·s-1·cm-2·K-4), and T the absolute temperature (K) of the object. Cm242 has a radioactive decay heat of 122 W/g. If a sphere of pure, solid Cm242 metal is floating in deep space far from any heat sources, how large must the sphere be (diameter in centimeters) to melt itself from its own decay heat?

24.5. In the gaseous diffusion process, a very large number of holes smaller than 50 nm in diameter are needed in each barrier to achieve efficient isotopic separation of U235 from U238. Propose a method to produce Ni barriers that would have large numbers of holes smaller than 50 nm.

24.6. The fission of one U235 atom releases about 200 MeV of energy. It is estimated that the world’s U reserves contain 2 billion metric tons of U that could be recovered profitably if the cost of U were $80/kg. Calculate the total energy that could be released if all this U235 were fissioned, and compare that value to the 4.5 x 1020 J of energy used by all of humankind from all sources on Earth per year.

24.7. Make a copy of Fig. 24.3 and draw on this illustration the position of the -U twin plane and a vector representing the shear direction of twinning on this plane.

24.8. Pu metallurgists have often stated that the various odd physical properties of Pu make it the most difficult of all metals to work with. However, there is one attribute of the -stabilized Pu–Ga alloys that actually makes them easier to cast than most metals. Figure 24.8 shows the relation between length and temperature behavior of pure Pu. The behavior of the and phases in -stabilized Pu–Ga alloys is very similar to the behavior shown in Fig. 24.8. Use Fig. 24.8 and the information given in Sec. 24.5 to help you formulate a statement explaining why Pu–Ga alloys are easier to cast than most metals.

24.9. Inhalation of 40 ng of Pu238 causes a significant increase in the risk of developing lung cancer. Calculate the volume of a piece of Pu238 metal having a mass of 40 ng. A typical grain of beach sand is a cube about 0.3 mm on a side. Compare the volumes of a 40 ng mass of Pu238 metal with that of a grain of sand.

24.10. In Sidebar 24.2 we described an experiment in which a U rod was cycled 1300 times between 50 and 550˚C. This thermal cycling distorted the rod severely. Predict what would happen if a piece of pure Pu were subjected to the same 1300 cycles between 50 and 550˚C, and explain the reasoning behind your prediction.

- 25.1. The NiAl intermetallic has the crystal structure shown in Fig. 25.3. The only slip direction that is known to operate during plastic deformation at room temperature is the <010> type.  The only slip planes that are known to operate during plastic deformation are the {100} and {101} families of planes. A single crystal of NiAl is tensile tested with the tensile axis parallel to the [111] direction.  The two active slip planes each have a critical resolved shear stress of 32 MPa.  (a) Use Schmid's law to calculate which slip system drawn in Fig. 25.3 would slip first, the (100)[010] or the (101)[010]. (b)  Predict the outcome of a tensile test performed on a single crystal of NiAl with the tensile axis oriented parallel to the [001] direction.  Explain how you reached your conclusion.

- 25.2. The AlRu cI2 intermetallic compound shows evidence of dislocations moving in the crystal with both <100> and <111> Burgers vectors. (a)  Discuss why this is unusual in comparison to typical cI2 intermetallic dislocation behavior. (b) Although polycrystalline AlRu shows high ductility in compression testing, its tensile ductility is lower. Suggest one or more mechanisms that could be acting in polycrystalline AlRu to cause low tensile ductility.

25.3. Intermetallic compounds could permit heat engines to operate at higher temperatures. (a)  Calculate the Carnot efficiency of a heat engine operating with a 1000˚C hot-side temperature and a 20˚C cold-side temperature. Repeat this calculation for the case of a 1200˚C hot-side temperature and a 20˚C cold-side temperature. (b)  If global fuel consumption in such heat engines is 1.0(1012) liters per annum, and the average fuel cost is $0.15 per liter, calculate the savings that would result from raising the hot side temperature from 1000˚ C to 1200˚C.

25.4. One of the challenges in galvanizing sheet steel is selecting the material of the roller that is immersed in the molten Zn (Fig. 25.10).  Bare steel tends to form intermetallic compounds with the Zn that gradually embrittle the metal, so an alternative material is needed either as bulk material or as a coating for steel rollers.  Recommend a material to be used for the roller or for a coating on steel rollers, and state why you feel the material you chose is a good choice from the following perspectives: (1) minimizing material reactivity with Zn, (2) minimizing cost, (3) maximizing the ability of the material to survive occasional impacts and cooling/heating between 20 and 450˚ C, and (4) the ability of the material to maintain reasonable strength and wear resistance (100 MPa yield strength at a temperature of 450˚C).

25.5. The tetragonal unit cell of the AuCu intermetallic compound is shown in Fig. 25.11.

(a) For each of the following slip systems, calculate the length of the Burgers vector needed to maintain a perfect ordered crystal (no antiphase boundaries) after one dislocation passes through the lattice: (1) (011)[011], (2) (111)[110], (3) (111)[101], and (4) (001)[110]. (b) Calculate the Burgers vectors lengths for the four slip systems listed in part (a) if antiphase boundaries are permitted. (c) Dislocation energy increases in proportion to the square of the Burgers vector length. Would the shortest Burgers vector case from all your answers in parts (a) and (b) be the slip system that you would expect to have the lowest dislocation energy in AuCu? Answer “yes”, “no”, or “there is not enough information to say with certainty” to this question, and justify your answer.

25.6. The pest oxidation problem is often seen in intermetallics, but it is rare in ordinary metals. Present a possible explanation for this difference in behavior.

25.7. When attempts are made to weld Fe to Al using inert-gas shielded electric arc welding, the metal in the weld's fusion zone always cracks as it cools. (a) Explain why this cracking occurs. (b) Suggest an alternative method to produce a metallic bond across the Al–Fe interface that will be free of cracks.

25.8. The rotation of a polycrystalline NiAl turbine blade in an experimental engine places a 50-MPa tensile stress on the blade. The heat of combustion raises its temperature to 800˚C. At 800˚C, the yield strength of NiAl is greater than 50 MPa. The coefficient of thermal expansion of NiAl is 15.1(10-6) K-1. (a) Use this information and Fig. 25.1 to estimate the change in length (l) of the blade if its length is 3.00 cm when the engine is at rest at room temperature. (b) After the calculation in part (a) is performed, an engineer suggests that the exterior housing be placed (3.00 + l) cm from the inner edge of the blade so there will be no “blow-by” leakage of gas past the outer tip of the blade. Comment on the advisability of this suggestion.

25.9 The room-temperature ductility of the RM rare earth cI2 intermetallics (Sec. 25.9.2) has elicited scientific interest but relatively little engineering interest. Briefly explain why the RM intermetallics would be difficult to use in high-temperature applications.