## Slide 1: RELIABILITY: CHAPTER 6
MODELING COMPONENT FAILURES - II
PHYSICS OF FAILURE

## Slide 2: FAILURE OF PARTS
The failure of a part occurs due to a complex set of interactions between the material properties of the part and the stresses that act on the part. The process through which these interact and lead to a part failure is complex and is different for different types of parts (e.g., electrical, mechanical).
Two main types: OVERSTRES and WEAROUT failures

## Slide 3: OVERSTRESS FAILURES
In this case, an item fails only if the stress to which the item is subjected exceeds the strength of the item. If the stress is below the strength, the stress has no permanent effect on the item.
Stress can be mechanical, electrical, thermal, and so on.

## Slide 4: WEAROUT FAILURES
In this case, the stress causes damage that usually accumulates irreversibly. The accumulated damage does not disappear when the stress is removed, although sometimes annealing is possible. The cumulative damage does not cause any performance degradation as long as is it below the endurance limit. Once this limit is reached, the item fails.

## Slide 5: EFFECT OF STRESSES
The effects of stresses are influenced by several factors:
- geometry of the part
- constitutive and damage properties of the materials
- manufacturing
- operational environment

## Slide 6: OVERSTRESS FAILURES
Brittle fracture
Ductile fracture
Yield
Buckling
Large elastic deformation
Interfacial de-adhesion

## Slide 7: WEAROUT FAILURES
Wear
Corrosion
Dendritic growth
Interdiffusion
Fatigue crack propagation

## Slide 8: WEAROUT FAILURES [Cont.]
Diffusion
Radiation
Fatigue crack initiation
Creep
Electromigration

## Slide 9: LARGE ELASTIC DEFORMATION
Elastic deformation typically occurs in slender items. Failure is due to excessive deformation under overstress. Being elastic, the deformations are reversible and therefore do not cause any permanent change in the material.
Examples: Large antennas, solar panels.

## Slide 10: YIELD
A component that is stressed past its yield strength results in an irreversible plastic strain and leads to a permanent deformation due to a permanent change in the material. This phenomena most often occurs in components made of metals which are ductile and crystalline.
Example: Spring

## Slide 11: BUCKLING
Buckling is a phenomenon that occurs in slender structures under compressive overstress. Deformation in the direction of the compressive load can suddenly change at a critical point, resulting in an instantaneous and catastrophic deformation in a direction perpendicular to the loading direction.

## Slide 12: BRITTLE FRACTURE
In brittle materials (such as glass and ceramics), high stress concentration can occur at local microscopic flaws under overstress. This excessive stress can cause a failure by sudden catastrophic propagation of the dominant micro-flaw.

## Slide 13: DUCTILE FRACTURE
In ductile fracture, the failure is due to sudden propagation of a pre-existing crack in the material under external stress. It differs from brittle fracture in the sense that there is large-scale yielding at the tip of the crack which preceded the crack propagation.

## Slide 14: INTERFACIAL DE-ADHESION
Interfacial de-adhesion occurs at the interface between two adhering materials. One of the factors enhancing this between two dis-similar materials is interdiffusion. The interfacial strength depends on the chemical and mechanical properties of the interface.
Examples: Composite materials

## Slide 15: FATIGUE CRACK INITIATION AND GROWTH
When a component is subjected to a cyclic stress, failure usually occurs at stresses much below the ultimate tensile strength and is due to accumulation of damage. Such failures are a result of incremental damage that occurs during each load cycle and accumulates with the number of cycles. Failures of this type are termed fatigue failures.

## Slide 16: FATIGUE FAILURES
Fatigue failure is comprised of two stages
- crack initiation, and
- crack propagation.
A crack develops at a point of discontinuity (bolt hole, flaw)
Once initiated the crack grows under cyclic loading
Examples: airframes, bridges

## Slide 17: DIFFUSION AND INTERDIFFUSION
Diffusion is a mass transport process at the atomic level and interdiffusion is a mutual mass transfer process which occurs when two species intermingle at an interface.
Failures due to creep, corrosion, etc., are driven by diffusion phenomena.

## Slide 18: CREEP
Creep is a time dependent deformation. It differs from plastic and elastic deformation in terms of the time scales for the deformations to occur. In creep, the time scales are orders of magnitude larger. The deformation mechanism in polymers is different from those in metals and ceramics because of their special microstructure.

## Slide 19: CORROSION
Corrosion is the process of chemical or electrochemical degradation of materials.
Three common forms of corrosion:
- uniform corrosion
- galvanic corrosion
- pitting corrosion

## Slide 20: UNIFORM CORROSION
The reactions occurring at the metal-electrolyte interface are uniform over the surface of the item. Continuation of the process depends on the nature of the corrosion product and the environment. If the corrosion product is washed off or otherwise removed, fresh metal is exposed for further corrosion.

## Slide 21: GALVANIC CORROSION
Galvanic corrosion occurs when two different metals are in contact. In this case one acts as a cathode (where a reduction reaction occurs) and the other as an anode (where corrosion occurs as a result of oxidation).

## Slide 22: PITTING CORROSION
Pitting corrosion occurs at localized areas and results in the formation of pits. The corrosive conditions inside the pit accelerate the corrosion process.

## Slide 23: CORROSION [Cont.]
Corrosion reduces the fracture strength of the material
Corrosion is a very pervasive problem in some engineering environments
Examples: off-shore rigs operating in a salty environment, chemical plants

## Slide 24
ALLOY
AND
ENVIRONMENT
BREAKDOWN
OF
CORROSION
PREVENTION
MEASURES
INITIATION OF
CORROSION
METAL
LOSS
GROWTH OF
CORROSION
PRODUCTS
LOCALISED
CORROSION
STRESS
CONCENTRA
-TION
CRACK
INITIATION
& GROWTH
LEAK
UNIFORM
CORROSION
REDUCTION
OF
STRENGTH
LOOSENING
OF
FITTINGS
MECHANICAL
FAILURE
DETERIORATION
OF
APPEARANCE
WEDGING
OR
STICKING
CONTAMINATION
OF PROCESS
FLUID
CORROSION FAILURE MODES

## Slide 25: WEAR
Wear is the erosion of material resulting from the sliding motion of two surfaces under the action of a contact force. Erosion can be due to physical and chemical interactions between the two surfaces. The various microscopic physical processes, by which the particles are removed as wear debris, are called wear mechanisms.

## Slide 26: WEAR [Cont.]
Five categories of wear:
- adhesive
- abrasive (when a hard material is sliding against a soft material)
- surface-fatigue
- corrosive (chemical)
- thermal (mainly in polymers).

## Slide 27: MECHANICAL FAILURES
As a result of
elastic and plastic deformation,
buckling,
brittle and ductile fracture,
fatigue crack initiation and crack growth, and
creep and creep rupture.

## Slide 28: ELECTRICAL FAILURES
As a result of
electrostatic discharge,
dielectric breakdown,
junction breakdown in semiconductor devices,
hot electron injection,
surface and bulk trapping, and
surface breakdown.

## Slide 29: THERMAL FAILURES
As a result of
heating beyond critical temperatures (e.g., melting point), and
thermal expansions and contractions

## Slide 30: RADIATION FAILURES
As a result of
radioactive containments, and
secondary cosmic rays.

## Slide 31: CHEMICAL FAILURES
As a result of
corrosion,
oxidation, and
surface dendritic growth.

## Slide 32: FAILURE CLASSIFICATION
Degradation
Cracking Mechanical
Deformation
Wear
Corrosion
Fouling Chemical

## Slide 33: STRESS/STRENGTH MODELS
X: Strength of a part
Y: Stress on the part
X < Y implies failure of the part
X > Y implies the reverse
Note: Stress and strength can be mechanical, electrical or thermal depending on the part

## Slide 34: STRESS/STRENGTH MODELING
Strength (X) and Stress (Y) can be
- Deterministic or Random
- Static or Dynamic
Static: X and Y do not change with time
Dynamic: X and/or Y change with time

## Slide 35: STATIC MODEL
X is a random variable with distribution FX(x)
Y is deterministic
R: Reliability of product
R = P{X > Y} = 1 - P{ X < Y} = 1- Fx(Y)
As Y increases [decreases] R decreases [increases]

## Slide 36: STATIC MODEL [Cont.]
Both X and Y are random variables with distribution FX(x) and FY(y), respectively
Two approaches to computing the reliability R
Approach 1: Define Z = X - Y and let FZ(z) denote the distribution of Z
Then R = P{Z > 0} = 1 - FZ(0)

## Slide 37: STATIC MODEL [Cont.]
Approach 2: Uses the conditional approach.
Conditional on Y = y, we have
On removing the conditioning, we have

## Slide 38: STATIC MODEL [Cont.]
which can also be written as

## Slide 39: EXAMPLE
Suppose that both X and Y are normally distributed -- i.e.,
X: N( X, ) and Y: N( Y, )
Then Z is also normally distributed with mean mean Z =X -Y and

## Slide 40: EXAMPLE [Cont.]
where  is the standard normal distribution with mean = 0 and variance = 1.

## Slide 41: EXAMPLE [Cont.]
Due to uncertainty in the load, the stress that a mechanical component is subjected to is normally distributed with a mean of 10 and a standard deviation of 3. Due to uncertainty in the manufacturing process, the strength of the component is also normally distributed with a mean of 25 and a standard deviation of X.
Note that if X = 5, = 0.995

## Slide 42: EXAMPLE [Cont.]
The following are values of R for a range of
3 4 5 6 7 8
R 0.9998 0.9987 0.9950 0.9873 0.9756 0.9604
As can be seen, the reliability decreases as increases, as is to be expected.

## Slide 43: DYNAMIC MODELS
Many different models, depending on how X and/or Y change with time
The effect of stress can be either cumulative (wear process) or not.
We consider two simple models (Model 1 and Model 2)
We need concepts from stochastic processes for modeling.

## Slide 44: STOCHASTIC PROCESSES
Earlier we defined a random variable as a function X() which maps events into a real line.
A stochastic process is a natural extension and is given by X(t, ) which is interpreted as follows.

## Slide 45: STOCHASTIC PROCESSES
For a defined event , it is a function of time t (implying that events are defined over time).
For a fixed t, it is a random variable.
Often,  is omitted so that X(t, ) is simply denoted X(t).

## Slide 46: STOCHASTIC PROCESSES
The probabilistic characterization of a stochastic process at ti, i = 1, 2, ...., n requires a n-dimensional distribution function
For a process with “Markov” property, this can be done in terms of a distribution function involving only two different time instants.

## Slide 47: STOCHASTIC PROCESSES
Some of the more important stochastic processes of relevance to reliability theory are
- Point Processes
- Counting Processes
- Renewal Processes
Several other types of processes are also used in modeling.

## Slide 48: POINT PROCESS
A point process is a continuous time stochastic process characterized by events which occur randomly along the time continuum.
Example: Number of failures over a time interval.

## Slide 49: COUNTING PROCESS
A point process {N(t), t  0} is a counting process if it represents the number of events that have occurred till time t. It must satisfy:
i) N(t)  0.
(ii) N(t) is integer valued.

## Slide 50: COUNTING PROCESS
(iii) If s < t, then N(s)  N(t).
(iv) For s < t, {N(t) - N(s)} is the number of events in the interval (s,t].
For the stationary Poisson Process

## Slide 51: COUNTING PROCESS
Non-stationary Poisson Process

## Slide 52: COUNTING PROCESS
Non-stationary Poisson Process
The expected number of failures in [0,t) is given by
Note: When (t) = , this becomes a stationary Poisson process with mean
M(t) = t.

## Slide 53: RENEWAL PROCESS
A counting process {N(t), t  0} is an ordinary renewal process if
(i) N(0) = 0. (ii) X1, the time to occurrence of the first event (from t = 0) and Xj, j  2, the time between the (j-1)st and jth events, are a sequence of independent and identically distributed random variables with distribution function F(x).

## Slide 54: RENEWAL PROCESS
(iii) N(t) = Sup {n: sn  t}, where
Note: The stationary Poisson process is a special case with F(x) an exponential distribution.

## Slide 55: RENEWAL PROCESS
The expected number of renewals in [0,t), M(t), is given by
It can be shown that

## Slide 56: DEGRADATION OVER TIME
x*
FAILURE TIME
T
X(t)
t

## Slide 57: CUMULATIVE DAMAGE
FAILURE
T1
T2
T3
T
t
x*
X(t)

## Slide 58: MODEL - 1
X deterministic (constant)
Y is a marked point process. This models shocks occurring randomly over time and the stress from each shock is a random variable.
Failure occurs the first instant when Y > X.

## Slide 59: Model - 1 [Cont.]
Shocks occur according to a Poisson process with intensity 
The stress (Y) from each shock is a random variable with distribution G(y)
The strength X is deterministic
T: The time to failure is a random variable with distribution H(t)

## Slide 60: Model - 1 [Cont.]
Let N(t) denote the number of shocks
received in [0, t).
Conditional on N(t) = n, we have
[stress due to each shock is less than X.]

## Slide 61: Model - 1 [Cont.]
On removing the conditioning, we have

## Slide 62: Model - 1 [Cont.]
Define  = G(x). Then H(t) = 1 - P{T > t} is given by
The mean time to failure is given by

## Slide 63: Model - 1 [Cont.]
As X increases (i.e., the component becomes stronger),  increases and, as a result, the mean time to failure also increases.
As  decreases (shocks occur less frequently), the mean time to failure increases.

## Slide 64: MODEL - 2
Each shock causes a damage which is additive (e.g., crack growth)
X(t) represent the total damage till time t
Failure occurs when X(t) exceeds a specified value x*.
x* depends on the design parameters
Changes to X(t) can be modeled in many different ways

## Slide 65: MODEL - 2 [Cont.]
Shocks occur according to a Poisson process with intensity 
Shock i does an amount of damage Xi which is a random variable with distribution G(x)
N(t) is the number of shocks till time t

## Slide 66: MODEL - 2 [Cont.]
Let T denote the time to failure. It is given by
Let H(t) denote the distribution function for T. It is obtained using the conditional approach as in Model 1.

## Slide 67: MODEL - 2 [Cont.]
Conditioning on N(t) = n, we have
The conditional probability is given by

## Slide 68: MODEL - 2 [Cont.]
where G(n)(x) is the n-fold convolution of G(x) with itself.

## Slide 69: MODEL - 2 [Cont.]
and, after some analysis,

## Slide 70: MODEL - 2 [Cont.] [Special Case]
F(t) and G(x) are both exponential
Then, H(t) is given by complicated function involving a Bessel function of order 1, I1( ).

## Slide 71: MODEL - 2 [Cont.] [Special Case]
The failure distribution is given by
The failure rate is given by

## Slide 72: PROPORTIONAL HAZARD MODEL
FAILURE RATE
time
t1
t2
EFFECT OF COVARIATES
}
}
BASELINE FAILURE RATES
OBSERVED FAILURE RATES